1	Disintegration  and  cancer  immunotherapy  efficacy  of  a  squalane-in-water  antigen

2

3

4	delivery system emulsified by bioresorbable poly(ethylene glycol)-block-polylactide

5

6

7

8

9	Wei-Lin Chen a,b, Shih-Jen Liu b, c, Chih-Hsiang Leng b, c, Hsin-Wei Chen b, c, Pele Chong b, c, Ming-Hsi Huang a,b,*

10

11

12

13

14

15

16	a  Graduate  Institute  of  Life  Sciences,  National  Defense  Medical  Center,  11466  Taipei,

17

18	Taiwan

19

20

21	b  National  Institute  of  Infectious  Diseases  and  Vaccinology,  National  Health  Research

22

23	Institutes, 35053 Miaoli, Taiwan

24

25       c Graduate Institute of Immunology, China Medical University, 40402 Taichung, Taiwan

26

27

28	* Corresponding author. Tel.: +886 37 246166#37742; fax: +886 37 583009.

29

30

31	E-mail address: huangminghsi@nhri.org.tw

32

33

34

35

36

37

38

39

40

41

42

43

44

45

46

47

48

49

50

51

52

53

54

55

56

57

*Abstract

Click here to download Abstract: 4Abstract_20130907.doc

1	ABSTRACT

2

3

4	Vaccine adjuvant is conferred on the substance that helps to enhance antigen-specific immune

5

6	response. Here we investigated the disintegration characteristics and immunotherapy potency

7

8

9	of the emulsified antigen delivery systems comprising bioresorbable polymer poly(ethylene

10

11	glycol)-polylactide  (PEG-PLA),  phosphate  buffer  saline  (PBS),  and  metabolizable  oil

12

13	squalane. PEG-PLA-stabilized oil-in-water emulsions show good stability at 4oC and at room

14

15

16	temperature. At 37oC, squalane/PEG-PLA/PBS emulsion with oil/aqueous weight ratio of 7/3

17

18	(denominated PELA73) was stable for 6 weeks without phase separation. As PEG-PLA being

19

20

21	degraded, 30% of free oil at the surface layer and 10% of water at the bottom disassociated

22

23	from the PELA73 emulsion were found after 3 months. The emulsion showed favorable for

24

25

26	both  storage  and  post-injection.  As  adjuvant  for  immunotherapeutic  use,  an  HPV16  E7

27

28	peptide  antigen  formulated  with  PELA73  plus  CpG  immunostimulators  could  strongly

29

30

31	enhance antigen-specific T-cell responses as well as anti-tumor ability with respected to

32

33	non-formulated or Alum-formulated peptide.

34

35

36

37

38	Keywords:

39

40	Bioresorbable polymer

41

42

43	Cancer immunotherapy

44

45	Emulsion disintegration

46

47

48	Tumor-associated antigen

49

50	Vaccine adjuvant

51

52

53

54

55

56

57

58

59

60

61

*Manuscript

Click here to download Manuscript: 5Manuscript_20130907.doc	Click here to view linked References

1	1. Introduction

2

3

4	A vaccine contains an agent dubbed antigen that resembles a disease-causing pathogen

5

6	(e.g. bacterium, virus, or toxin) to elicit adaptive immune responses. Vaccines have been

7

8

9	commonly applied to induce prophylactic immunity against infectious pathogens [1]. For

10

11	therapeutic  ends,  there  is  a  trend  to  generate  information  derived  from  immunology to

12

13

14	develop  therapeutic  vaccines  or  immunotherapy  technology  against  pathogen-associated

15

16	cancers [2], and immune dysfunctions such as chronic inflammation and autoimmune disease

17

18	[3].  Ideally,  cancer  immunotherapy  utilizes  tumor-associated  antigens  to  produce  robust

19

20

21	immunity and antitumor efficacy. However, recombinant protein or epitope peptide-based

22

23	immunotherapies   have   faced   limited   clinical   success   caused   by  the   relatively  low

24

25

26	immunogenicity, and hence require the incorporation of adjuvants to elicit efficient cytotoxic

27

28	T lymphocyte (CTL) activities against tumor cells [4,5].

29

30

31	Emulsion delivery systems have been widely used in the immunotherapy and vaccine

32

33	development to enhance immune responses to co-administered antigens [6]. In contrast to

34

35	water-in-oil  (W/O)  emulsions,  which  foster  local  reactions  at  the  injection  site,  O/W

36

37

38	emulsions have the advantages of low oil content and high injectability when performing

39

40	vaccination [7]. Regarding the mechanisms of adjuvant action, O/W emulsions possess high

41

42

43	efficiency to the induction of an early and strong cytokine- and chemokine-rich environment

44

45	at the site of injection, and beneficial of modulation of genes involved in leukocyte migration

46

47

48	and antigen presentation [8,9]. We have previously studied on the engineering of amphiphilic

49

50	bioresorbable polymers as a promising strategy for the delivery of vaccine antigens and/or

51

52	immunostimulatory molecules [10,11]. Ideally, bioresorbable polymeric emulsifiers, with a

53

54

55	hydrophobic block that is degradable, show bulk degradation and further resorb in vivo. This

56

57	allows  stabilization  of  emulsion  particles  during  storage,  however,  disintegration  of  the

1	system post-injection. Immunogenicity studies in mice by using ovalbumin and influenza as

2

3

4	model showed that bioresorbable polymers-stabilized emulsions are able to induce potent

5

6	antibody responses [10-13].

7

8

9	The degradation rate of a bioresorbable polymer implant has been shown to correlate

10

11	with cell vitality, cell growth and host response [14], it is relatively important to evaluate the

12

13

14	degradation characteristics as well as the final products of the designed polymer for those

15

16	applications in biomedical use. In addition, whether degradation of polymeric emulsifier can

17

18	turn on the emulsion disintegration during storage and post-injection is still unknown. To the

19

20

21	best of our knowledge, the detail degradation characteristics of PEG-PLA were not fully

22

23	investigated  by  matrix-assisted  laser  desorption/ionization  time-of-flight  (MALDI-TOF)

24

25

26	technology. In this study, we plan to study the relation between degradation of polymer and

27

28	disintegration of emulsion. Moreover, it was interesting to study on whether the bioresorbable

29

30

31	polymer-based vaccine adjuvant can enhance the cell-mediated responses elicited by peptide

32

33	antigen so as to be used as immunotherapy tool in suppressing tumor growth. Degradation of

34

35	PEG-PLA was carried out in pure water at 25°C and 37°C selected to mimic the usual storage

36

37

38	conditions and the post-administration stage, and followed by analytical techniques such as

39

40	gel  permeation  chromatography  (GPC)  and  MALDI-TOF  mass  spectrometry.  In  vivo

41

42

43	distribution  was  investigated  in  mouse  model  to  elucidate  the  targeting  delivery  of

44

45	antigen-loaded  systems  bearing  fluorescence.  The  immunogenicity studies  in  mice  were

46

47

48	investigated by assessing the anti-tumor T cell responses as well as the effectiveness of these

49

50	responses in inducing tumor regression. These results were compared with those obtained

51

52	from conventional aluminum-based mineral salts (Alum) adjuvant.

53

54

55

56

57	2. Materials and methods

1	2.1. Materials

2

3

4	DL-lactide was purchased from Aldrich (Seelze, Germany) and recrystallized from ethyl

5

6	acetate. Polyethylene glycol 2000 monomethyl ether (MePEG2000) was supplied by Fluka

7

8

9	(Buchs, Switzerland) and used as received. Tin(II) 2-ethylhexanoate (SnOct2), phosphate

10

11	buffer	saline	(PBS),	squalane,	α-cyano-4-hydroxycinnamic	acid	(CHCA),	sodium

12

13

14	trifluoroacetate (Na-TFA), dimethyl sulfoxide-d6 (DMSO-d6) were purchased from Sigma

15

16	(St.  Louis,  Missouri,  USA).  All  solvents  were  of  analytical  grade.  AB-type  diblock

17

18	copolymer PEG-PLA was synthesized by ring-opening polymerization of DL-lactide in the

19

20

21	presence of MePEG2000 and SnOct2, as described previously [11].

22

23

24

25

26	2.2. Degradation of PEG-PLA

27

28	5 mg of PEG-PLA was dissolved in the eppendorf tube filled with 100 μL of distilled,

29

30	deionized water. The tubes were placed either at room temperature (25oC) or in a circulating

31

32

33	water  bath  at  37oC.  At  predetermined  time  points,  three  specimens  were  collected  and

34

35	lyophilized before being subjected to analyses.

36

37

38

39

40	2.3. Measurements

41

42

43	GPC was performed by using a setting composed of an isocratic pump, a refractive

44

45	index (RI) detector, and two size exclusion columns connected in series, one PLgel 5 μm

46

47

48	guard column (7.5 × 50 mm), and one PLgel 5 μm mixed-D column (7.5 × 300 mm). The

49

50	mobile phase was tetrahydrofuran (THF) and the flow rate was 1.0 mL/min. Data were

51

52	expressed with respect to polystyrene standards (Varian, Inc., Amherst, MA, USA). 1H-NMR

53

54

55	spectra was recorded at room temperature with a Varian VXR 300 MHz spectrometer (Varian,

56

57	Palo Alto, CA, USA) using DMSO-d6  as solvent and tetramethylsilane as shift reference.

58

59

60

61

1	Mass spectra were acquired by using the Micromass®  MALDI micro MXTM Time of Flight

2

3

4	Mass Spectrometer (Waters®, Milford, MA, USA) in the reflection mode. 1 μL aliquot of

5

6	degradation samples were premix with 1 μL of 0.2% TFA/acetonitrile and mixed with CHCA

7

8

9	as the matrix and Na-TFA as the dopant. 1 μL aliquot of sample solutions were spotted on a

10

11	MALDI sample plate and air-dried to form a thin matrix/analyte film. The degraded samples

12

13	without the matrix were deposited onto a plate containing porous silicone spots (Waters®

14

15

16	MassPREPTM DIOS-targetTM Plate, Milford, MA, USA) to monitor the low molecular weight

17

18	components.

19

20

21

22

23	2.4. Polymer-stabilized emulsions

24

25

26	20 wt. % of PEG-PLA/PBS was mixed with squalane oil in three oil/aqueous weight

27

28	ratios: 3/7, 5/5 and 7/3. The mixtures were then emulsified using a Polytron®  PT 3100

29

30

31	homogenizer (Kinematica AG, Swiss) at 6,000 rpm for 5 min. The resulting emulsions were

32

33	served as stock for further characterizations such as the stability, the dispersion type, and the

34

- o	o

- particle size. The stability of emulsions was recorded by placing each sample at 4 C, 25 C

37

38	and 37oC, and then noted the visual aspects. The dispersion types of the emulsions were

39

40	measured by using an ES-51® conductivity meter (HORIBA, Kyoto, Japan). The emulsion

41

42

43	was re-dispersed in PBS and then applied to monitor the particle size by optical microscope

44

45	(Olympus  DP70,  Olympus  Inc.,  Tokyo,  Japan)  and  by  laser  light  scattering  technique

46

47

48	(Brookhaven 90 plus particle size analyzer, Brookhaven Instruments Limited, NY, USA).

49

50

51

52	2.5. Peptides and cell line

53

54

55	Peptide used in this study is a H-2Db-restricted (RAHYNIVTF; RAH) CTL epitope

56

57	derived from the human papillomavirus (HPV) type 16 E7 protein, and was synthesized

58

59

60

61

1	in-house by solid phase method using an automated peptide synthesizer (Prelude™, Protein

2

3

4	Technologies  Inc.,  Tucson,  AZ,  USA),  employing  the  Fmoc  group  for  α-amino  group

5

6	protection. The purity was >90% for all of the peptides.

7

8

9	Murine epithelial cell line transformed with the oncogenes Ras and HPV-16 E6 and E7,

10

11	TC-1 (ATCC number: CRL-2785™), was maintained in RPMI 1640 medium supplemented

12

13

14	with 2 mM L-glutamine, 1.5 g/L sodium bicarbonate, 4.5 g/L glucose, 10 mM HEPES, 1 mM

15

16	sodium pyruvate, and 10% fetal bovine serum (JRH Biosciences, Lenexa, KS, USA).

17

18

19

20

21	2.6. Mice and ethic statement

22

23	Six-to-eight   week-old   female  C57BL/6   mice  were  obtained  from  the  National

24

25

26	Laboratory Animal Center. All mice were housed at the Laboratory Animal Facility of the

27

28	NHRI, Miaoli County, Taiwan. All animal studies were approved by the NHRI Institutional

29

30

31	Animal Care and Use Committee (NHRI-IACUC-098010-A).

32

33

34

35	2.7. Immunization and T-cell immunity

36

37

38	Mice were immunized s.c. with 30 μg of RAH peptide in PBS or formulated with 300

39

40	μg/dose of aluminum phosphate suspension (ADJU-PHOS®, Brenntag AG, Frederikssund,

41

42

43	Danish)  or  10  μg/dose  of  CpG  (5'-TCC  ATG  ACG  TTC  CTG  ACG  TT-3'  with  all

44

45	phosphorothioate  backbones;  synthesized  by  Invitrogen  Taiwan  Ltd.)  or  PELA73  or

46

47

48	PELA73/CpG combination adjuvant. The PELA73-containing formulations were investigated

49

50	by re-dispersing 100 µL of stock PELA73 emulsion into 900 µL of vaccine bulk before

51

52	injection.

53

54

55	Seven days after injection, spleen from the immunized mice was collected and cell

56

57	suspensions were harvested followed by resuspended in ACK lysis buffer (consisting of 155

58

59

60

61

1	mM NH4Cl, 10 mM KHCO3, 0.1 mM EDTA) for 1 min. Single cell suspensions (5x105 cells)

2

3

4	were re-stimulated in triplicate in the presence or absence of 10 μg/mL target RAH peptide.

5

6	Interferon (IFN)-γ- and interleukin (IL)-4-secreting cells were analyzed by enzyme-linked

7

8

9	immunosorbent spot (ELISPOT) assay (eBioscience, San Diego, USA) and the concentration

10

11	of released cytokine in culture medium was quantified by enzyme-linked immunosorbent

12

13

14	assay (ELISA) (R&D systems, Minneapolis, Minnesota, USA).

15

16	For  ELISPOT analysis,  cells  and  medium  were decanted  from  the  capture  antibody

17

18	coated plates after culturing in a 5% CO2  incubator at 37oC for 3 days. After washing,

19

20

21	biotinylated detection antibody was added to the plates and incubated at room temperature for

22

23	2 hrs and then the antibody solution was decanted. After another 45 mins of incubation at

24

25

26	room  temperature  with  Avidin-HRP conjugate,  freshly  prepared  AEC  substrate  solution

27

28	(Sigma, Saint Louis, MO, USA) was added and allowed to develop color at room temperature

29

30

31	for 40 minutes. By monitoring development of spots, the substrate reaction was stopped by

32

33	washing  wells  3  times  with  distilled  water.  The  spots  were  then  counted  by  using  an

34

35	automated ELISPOT plate reader (Cellular Technology Ltd., Shaker Heights, OH, USA). The

36

37

38	numbers of cytokine-secreting splenocytes were calculated as the average of spots in the

39

40	triplicate stimulant wells. Cell-depleted supernatants were analyzed by ELISA development

41

42

43	kit  using  paired  antibodies  following  the  manufacturer's  instructions.  The  assay  was

44

45	developed by adding aqueous tetramethylbenzidine substrate solution (TMB, NeA-Blue®,

46

47

48	Clinical Science Products, Inc. Mansfield, MA, USA), and the reaction was stopped in 2N

49

50	H2SO4. Plates were read at 450 nm on an ELISA plate reader (Molecular Devices, Sunnyvale,

51

52	CA, USA).

53

54

55

56

57	2.8. Tumor challenge study

58

59

60

61

1	Mice were first inoculated s.c. with 2×105  or 5×105/mouse TC-1 tumor cells into the

2

3

4	flank. Upon the appearance of palpable tumors, the C57BL/6 mice were injected s.c. at the

5

6	base of the tail with 10 µg of RAH peptide on day 7. Tumor sizes were measured by using a

7

8

9	caliper (Digimatic Caliper, Mitutoyo, Japan) in two vertical dimensions two times per week.

10

11	Tumor  volumes  were  calculated  according  to  formula:  (length  x  width2)/2.  Mouse  was

12

13	euthanized when tumor volume exceeded 2,500 mm3  or severe faintness. Median survival

14

15

16	was calculated by Gehan-Breslow-Wilcoxon method.

17

18

19

20

21	2.9. Statistical analysis

22

23	The graphs and statistical analyses were performed using GraphPad Prism version 5.02

24

25

26	(GraphPad Software, Inc.). Comparison of survival curve between groups was calculated by

27

28	use of log-rank (Mauted-Cox) test. Comparison of T cell immune responses between groups

29

30

31	was determined by Mann-Whitney test. The differences were considered significant as P <

32

33	0.05.

34

35

36

37

38	2.10. IVIS Spectrum imaging analysis

39

40	Mice were injected subcutaneously (s.c.) at the dorsal region with 10 μg of RAH-Alexa

41

42

43	Fluor®647 (absorption 650 nm; fluorescence emission 668 nm, synthesized by GeneDireX®,

44

45	Taoyuan, Taiwan) or 10 µg of CpG-cy5 (absorption 650 nm; fluorescence emission 668 nm,

46

47	synthesized by GeneDireX®, Taoyuan, Taiwan) either with PBS (200 μL, control experiment)

48

49

50	or  supplemented  with  PELA73  emulsion  diluted  in  PBS  (20  μL/180  μL).  Mice  were

51

52	anesthetized with isoflurane at a maintenance concentration of 2.5%, and oxygen pressurized

53

54

55	at 4 kg/cm2 in conjunction with XGI-8 Anesthesia System. In-life fluorescence analysis was

56

57	performed at 7, 30, 48, 72, and 144 hrs after treatment using a Xenogen IVIS® Spectrum 200

58

59

60

61

1	Imaging System (Caliper Life Sciences, USA). The fluorescent measurement was quantified

2

3

4	using IVIS Living Image 4.0 software package.

5

6

7

8

9	3. Results

10

11	3.1. Formulation and physicochemical characterization of polymer-based emulsions

12

13

14	The emulsifier used here has initial molecular characteristics of 75 wt.% of hydrophilic

15

16	block PEG and 25 wt.% of lipophilic block PLA with GPC molecular weight of 2,500 daltons

17

18	and polydispersity of 1.1. Squalane was selected as the core oil because it is very stable and

19

20

21	not susceptible to oxidation. It is also referred biocompatible and metabolizable in human and

22

23	currently has been used as a skin moisturizer in cosmetics and as an adjuvant in vaccines [15].

24

25

26	Table  1  summarizes  the  physicochemical  characteristics  of  the  emulsified  formulations

27

28	comprising PBS, PEG-PLA copolymer, and squalane.

29

30

31	Dynamic light scattering showed the polymeric aqueous solution (20 wt.%) possessing a

32

33	unimodal distribution with an average diameter of 13 nm (Table 1), probably due to the

34

35	micelle formation of the block copolymer by packing of the hydrophobic PLA block [10]. By

36

37

38	incorporating the squalane into the polymeric aqueous solution, phase separation occurs due

39

40	to immiscible of squalane and water. Followed homogenization under gentle conditions, a

41

42

43	white  and  isotropic  emulsion  was  rendered.  We  thus  termed  the  PEG-PLA-emulsified

44

45	adjuvant as PELA37 when the oil/aqueous weight ratio being 3/7. Upon storage at room

46

47

48	temperature, 35% of water disassociated from the bottom of the PELA37 emulsion within 24

49

50	hrs, but beyond this, no further water disassociation from the emulsion occurred. Increasing

51

52	the squalane content could significantly enhance the stability of the squalane/water interface.

53

54

55	When oil/aqueous weight ratio being 7/3 (denominated PELA73), a stable emulsion was

56

57	formed without phase separation for at least 6 months' storage. Concerning the dispersion

58

59

60

61

1	type of the emulsions, it is generally recognized that an emulsion of zero conductivity will

2

3

4	tend to be water dispersed in the oil, otherwise oil dispersed in the water [16]. As listed in

5

6	Table 1, squalane and PBS have conductivity of 0 ms/m and 125 ms/m, respectively. The

7

8

9	electrolytic conductivity of the emulsions with different oil/aqueous ratios was measured as

10

11	61  ms/m  (PELA37),  24  ms/m  (PELA55),  and  12  ms/m  (PELA73),  indicating more  oil

12

13

14	content leads to lower conductivity. Moreover, the three emulsions were well dispersed in

15

16	aqueous  solution.  These  results  revealed  the  dispersion  type  of  squalane/PEG-PLA/PBS

17

18	emulsions belong to the O/W emulsion type. The particle size of the different oil/aqueous

19

20

21	ratio emulsions was further investigated by optical microscope and laser light scattering

22

23	technology. As shown in Fig. 1 and Table 1, squalane/PEG-PLA/PBS emulsions were general

24

25

26	unimodal  with  the  size  distribution  between  400  nm  to  500  nm  no  matter  what  the

27

28	oil/aqueous ratio changes.

29

30

31

32

33	3.2. Hydrolytic degradation of PEG-PLA and disintegration of PEG-PLA-based squalane

34

35	emulsion

36

37

38	Fig. 2A and 2B present the GPC and of MALDI-TOF profiles of PEG-PLA during

39

40	degradation in distilled deionized water at 37oC. The molecular weight (MW) decrease was

41

42

43	rapid at the early stages. The number-average molecular weight (Mn) decreased from initial

44

45	3,850 to 3,300 at week 2 and to 2,850 at week 6. Afterwards, the decrease rate slowed down.

46

47

48	Mn = 2,800 and 2,750 were detected after 3 months and 6 months respectively. To precisely

49

50	realize the degradation characteristics of the PEG-PLA block copolymer, we monitor the

51

52	detail molecular weight changes by MALDI-TOF mass spectrometry. As shown in Fig. 2B,

53

54

55	the MePEG2000  spectra was well resolved, and the peaks were separated by 44 mass units,

56

57	which corresponded to the MW of the EG monomer (oxyethylene units = 44.03 g/mol). After

58

59

60

61

1	polymerizing with DL-lactide, other peaks separated by 72 mass units appeared (lactyl units

2

3

4	= 72.06 g/mol), in agreement with the presence of PLA blocks. After 2 weeks' degradation at

5

6	37oC, the peaks corresponded to lactyl units strongly decreased, indicating the loss of PLA

7

8

9	component.  Beyond  3  months,  no  signal  characteristics  of  PLA  were  detected  on  the

10

11	MALDI-TOF mass spectra, in agreement with GPC data. In the absence of matrix-related

12

13

14	background, desorption-ionization mass spectrometry on porous silicon is able of monitoring

15

16	low molecular weight components released during degradation. On the MALDI-TOF spectra

17

18	of PEG-PLA (Fig. 2B), no peak corresponding to LA oligomers was detected in the range

19

20

21	between 100 m/z and 900 m/z at the very beginning, indicating the elimination of low

22

23	molecular weight species during purification. There was a burst at week 1, i.e. in the period

24

25

26	where important changes occurred. As degradation proceeded, the peaks of LA oligomers

27

28	kept high intensity at week 2 and week 6. However, there were no typical LA bands detected

29

30

31	on the spectrum beyond 3 months, in agreement with GPC data. MALDI-TOF data showed

32

33	that large amounts of PLA oligomers broke away from PEG-PLA between week 1 and 6.

34

35	Beyond,  ester  bond  cleavage  of  PLA  oligomers  takes  place  continuously  to  further

36

37

38	degradation, suggesting PLA preserved its degradability.

39

40	The degradation rate was strongly reduced as the temperature decreased from 37oC to

41

42

43	25oC. As shown in Fig. 3A, Mn decreased progressively from initial 3,850 to 3,550 at week 2

44

45	and to 3,350 at week 6. Mn  = 3,200 and 2,900 were detected after 3 months and 6 months

46

47

48	respectively. Similar features are noted for MALDI-TOF analysis (Fig. 3B). After two weeks,

49

50	PEG-PLA still showed similar MALDI distribution as the beginning, beyond, the decrease of

51

52	PLA  peaks  were  detected  from  6  weeks  to  6  months.  Very  small  amount  of  peaks

53

54

55	corresponding to PEG-PLA were still detectable under 6 months' degradation. Concerning the

56

57	low molecular weight species, the peaks of LA oligomers kept high intensity during the

58

59

60

61

1	whole degradation period, indicating a differentiation between 25oC and 37oC.

2

3

4	Since the  interface  between  squalane  and  PBS  was  stabilized  by the  bioresorbable

5

6	polymer PEG-PLA, we attempt to investigate the relationship between the degradation of

7

8

9	PEG-PLA and the stability of squalane/PEG-PLA/PBS emulsions. The emulsified PELA73

10

11	was separately incubated in 4oC, 25oC and 37oC and recorded the visual aspects. An isotropic

12

13	emulsion was sustained for 6 months of storage at 25oC (Fig. 3C) and last at least 1 year at

14

15

16	4oC. On the other hand, the bottom water layer and the surface free oil were dissociated from

17

18	the emulsion at 3 month and 6 month while incubated at 37oC (Fig. 2C). It is noteworthy that

19

20

21	the time points of the emulsion disintegration were correlated with the PEG-PLA degradation

22

23	profiles. To verify the disintegration of the emulsion was caused by the degradation of the

24

25

26	emulsifier PEG-PLA, we further analyzed the residues existed in the dissociated water layer

27

28	by  MALDI-TOF  mass  spectra.  Data  showed  that  peaks  corresponding  to  LA motif  in

29

30

31	PEG-PLA  were  fully  disappeared  in  the  residues,  i.e.  no  additional  peaks  other  than

32

33	MePEG2000 (see Supplementary information Fig. S1). These results indicate the loss of PLA

34

35	moiety of PEG-PLA directly affected the stability of PEG-PLA-stabilized emulsion, leading

36

37

38	to disintegration of PELA73 and phase separation of squalane/water.

39

40

41

42

43	3.3. Antigen-specific T-cell immune responses and tumor regression efficacy

44

45	HPVs  have  been  known  the  most  common  sexually transmitted  infections  and  are

46

47

48	responsible for most of cervical cancer cases [17]. We applied cancer immunotherapy of

49

50	RAHYNIVTF peptide/TC-1 cells as tumor-associated antigen/tumor cells model to evaluate

51

52	the adjuvanticity of PELA73 [18].

53

54

55	Firstly, RAH was s.c.-injected into C57BL/6 mice. Seven days after the immunization,

56

57	single-cell suspensions were prepared from the mouse spleen and re-stimulated in vitro in the

58

59

60

61

1	presence of peptide antigen. The cytokine-secreting responses were detected by ELISPOT

2

3

4	and ELISA assays. As shown in Fig. 4A, vaccination of 30 μg of RAH peptide alone or

5

6	formulated with PELA73 showed no effect on the enhancement of IFN-γ-secreting cells

7

8

9	compared with the naïve group. The group treated with conventional adjuvants such as Alum

10

11	and CpG ODN (oligodeoxynucleotide containing unmethylated cytosine-guanosine motifs;

12

13	[19]) induced higher spot numbers (75±6 and 126±9 spots per 106 splenocytes, respectively)

14

15

16	than peptide alone, indicating that the two adjuvants could trigger the RAH-specific T-cell

17

18	activation.  Interestingly,  the  highest  IFN-γ-secreting  cells  are  obtained  in  the  group  of

19

20

21	combination of PELA73 and CpG (387±7 spots per 106  splenocytes), which was 5 times

22

23	more than Alum and 3 times higher than CpG alone group. The present results indicate that

24

25

26	PELA73 emulsified particles probably could not act as immunostimulatory adjuvants for

27

28	immune cells, but as antigen delivery systems instead. Moreover, combination adjuvants

29

30

31	which consist of particulate delivery system PELA73 and immunostimulatory compound

32

33	CpG  can  be  regarded  as  an  interesting  alternative  to  deliver  antigen/immunostimulator

34

35	effectively to the receptors of the immune cells so as to integrate the immune responses of

36

37

38	RAH peptide. Fig. 4B showed the concentration of released IFN-γ in culture medium by

39

40	splenocytes after re-stimulated by peptides for 3 days. The same tendency as ELISPOT assay

41

42

43	was found, i.e. co-administration of RAH with the combination of PELA73 and CpG induced

44

45	the  most  IFN-γ  release  compared  with  those  adjuvanted  with  CpG,  PELA73,  or  Alum

46

47

48	adjuvant. Nevertheless, the IL-4 cytokine was found to be at the undetectable level.

49

50	The  tumor  challenge  was  carried  out  in  mouse  model  to  evaluate  the  therapeutic

51

52	potential of our adjuvant-formulated cancer vaccine. C57BL/6 mice were first inoculated

53

54

55	with 2×105/mouse TC-1 tumor cells then immunized RAH peptide at day 7. The tumor

56

57	volume and survival rate were followed and recorded in Fig. 5. Without any treatment (PBS

58

59

60

61

1	control group), tumors grew progressively and the mice started lethal within 30 days (Fig. 5A

2

3

4	and B). No protection was observed for the mice received RAH peptide alone. Peptide

5

6	adjuvanted with Alum slightly slowed tumor growth and prolonged survival, but all mice

7

8

9	were   still   lethal   before   day   60.   Vaccination   of   RAH   peptide   plus   CpG   as   the

10

11	immunostimulator provided better protective effect than adjuvanted with Alum, but still not

12

13

14	good enough to eliminate inoculated TC-1 cells. The mice received RAH peptide formulated

15

16	with PELA73 neither decreased the mortality nor reduced the tumor volume, nevertheless, it

17

18	is noteworthy the combination of PELA73 and CpG was able to efficiently eliminate most

19

20

21	TC-1 cells which was better than CpG alone. The average tumor volume of PELA73/CpG

22

23	group was less than 100 mm3  until day 52 with respect to day 38 in the CpG group. We

24

25

26	further challenge mice by inoculating 5×105/mouse TC-1 cells (i.e. 2.5 folds higher than

27

28	preliminary test) to distinguish the adjuvanticity between CpG alone  and PELA73/CpG.

29

30

31	Results showed that the mice received single injection of RAH (10 µg) adjuvanted with

32

33	PELA73/CpG strongly slow down the tumor volume increase when compared with those

34

35	adjuvanted with  CpG alone (Fig.  5C).  It is noteworthy the PELA73 really broaden the

36

37

38	immunostimulatory efficacy of CpG and prolong the median survival of TC-1-bearing mice

39

40	from 56 days to 92 days (Fig. 5D).

41

42

43

44

45	3.4. Biodistribution imaging of emulsified particles in mice

46

47

48	In vivo distribution was investigated in mouse model to elucidate the targeting delivery

49

50	of antigen-loaded systems bearing fluorescence, using Alexa Fluor®647-conjugated RAH

51

52	peptide  (RAH-Alexa  647)  as  model  antigen.  Mice  were  immunized  s.c.  with  10  μg

53

54

55	RAH-Alexa 647, either with antigen in PBS or adsorbed with PELA73 or PELA73/CpG. As

56

57	shown in Fig. 6A, the fluorescence signal was initially induced in the site of injection. At 7 hr,

58

59

60

61

1	the signal as shown in the representative image dropped dramatically in the RAH-Alexa

2

3

4	647-treated and PELA73/RAH-Alexa 647-injected mice. No signals characteristic of Alexa

5

6	Fluor® were detected on the IVIS spectra beyond 30 hr, indicating the absence of RAH-Alexa

7

8

9	647. The fluorescence signals of RAH-Alexa 647 are not influenced by the presence of

10

11	PELA73 nanoemulsion via subcutaneous route. However, we found that the fluorescence

12

13

14	signals of RAH-Alexa 647 via i.m. injection are strongly influenced by the presence of

15

16	PELA73 submicron emulsion, thus providing prolonged release profile of hydrophilic RAH

17

18	peptide. (see Supplementary information Fig. S2).

19

20

21	We also attempt to focus on the distribution of fluorescence-labeled CpG (CpG-cy5)

22

23	within PELA73 emulsified particles by the IVIS system. Mice were immunized s.c. with 10

24

25

26	μg CpG-cy5 either in PBS or formulated with PELA73. The fluorescence signals of CpG-cy5

27

28	in  PBS  were  dramatically  attenuated  after  30  hr  then  returned  to  baseline  within

29

30

31	approximately 144 hr following injection. On the other hand, the fluorescence signals were

32

33	only gradually decreased for the CpG-cy5/PELA73 injected mice (Fig. 6B).  Our results

34

35	demonstrated PELA73 provided a depot for bioactive agent CpG at injection site via s.c.

36

37

38	administration so as to prolong sufficient immunomodulatory responses against cancer.

39

40

41

42

43	4. Discussion

44

45	The synthesis and degradation profiles of bioresorbable polymer were monitored mainly

46

47

48	by the  GPC  chromatography  and/or  combined  with  NMR  method  [20-22].  However,  a

49

50	precise characterization of amphiphilic copolymer is not very easy because it is difficult to

51

52	distinguish on the NMR spectra whether the recovery samples are of copolymer form or a

53

54

55	mixture.  For  the  first  time,  we  investigate  the  hydrolytic  degradation  characteristics  of

56

57	amphiphilic PEG-PLA block copolymer by GPC and MALDI-TOF mass spectrometry. The

58

59

60

61

1	results  (Fig. 2 and Fig.  3)  indicate the time points of the emulsion disintegration were

2

3

4	correlated with the PEG-PLA degradation profiles. In addition, no signals characteristic of

5

6	LA were detected on the MALDI-TOF spectra of the residues existed in the dissociated water

7

8

9	layer, indicating the loss of PLA component. The loss of PLA moiety of the emulsifier

10

11	PEG-PLA  directly  affected  the  stability  of  PEG-PLA-stabilized  emulsion,  leading  to

12

13

14	disintegration of PELA73 and phase separation of squalane/water.

15

16	Vaccine adjuvants can be broadly separated into two classes based on their principal

17

18	mechanisms  of  action:  immunostimulatory  adjuvants  and  vaccine  delivery  systems.  In

19

20

21	contrast to the former which are thought to trigger a sufficient activation of the innate

22

23	immune systems, the latter are generally particulate and mainly function as a depot to ensure

24

25

26	the immunoavailability of antigen [23]. The conventional Alum adjuvant had been used many

27

28	decades and been shown to enhance antibody responses, however, often been considered a

29

30

31	poor adjuvant to induce CD8 T-cell activation [24,25]. Based on our immunogenicity and

32

33	tumor challenge studies, we also demonstrated antigen formulated with Alum can slightly

34

35	trigger  T cell  immune  response  (Fig.  4).  Unfortunately,  the  immunogenicity elicited  by

36

37

38	Alum-formulated RAH peptide was neither inhibit tumor growth nor tumor regression (Fig.

39

40	5A). To bypass these limitations, combination adjuvants which consist of particulate delivery

41

42

43	system and immunostimulatory compound can be regarded as an interesting alternative to

44

45	deliver antigen/immunostimulator effectively to the receptors of the immune cells and/or to

46

47	generate  the  number  of  the  receptors.  Prophylactic  CervarixTM   HPV  vaccine,  which  is

48

49

50	approved by US FDA, contains recombinant HPV type 16 L1 protein, type 18 L1 protein, and

51

52	combination	adjuvant	(dubbed	AS04)	comprising	of	aluminum	hydroxide	and

53

54

55	monophosphoryl lipid A. Some cross-reactive protection against virus strains type 31 and

56

57	type 45 were also shown in clinical trials [26]. On the other hand, it is well-documented in

58

59

60

61

1	literature that CpG oligodeoxynucleotides are agonists of intracellular receptor TLR9 that can

2

3

4	induce the activation of antigen presenting cells and Th1-dominated immune response [19].

5

6	However, CpG has been shown to be degraded rapidly in vivo by nucleases, leading to the

7

8

9	reduction of the desired immune response [27]; therefore, it requires some protecting vesicles

10

11	to prolong its efficacy. In the present study, we increase the immunogenicity of HPV16

12

13

14	E7(49-57) peptide antigen by using microencapsulation technology. PELA73 facilitates the

15

16	IFN-γ-secreting  responses  elicited  by  CpG  and  leading  to  generate  the  valuable  tumor

17

18	inhibition and tumor regression characters. In fact, IFN-γ is a predominant T helper type 1

19

20

21	(Th1) cytokine applicable to CTL activity against tumor cells [28], while IL-4 is a common T

22

23	helper  type  2  (Th2)  cytokine  relevant  tohumoral  immunity.  Effective  vaccination  was

24

25

26	correlated  with  the  induction  of  the  Th1  cytokines  (including  IFN-γ),  especially in  the

27

28	immunologically hyporesponsive populations such as the elderly and tumor-bearing host

29

30

31	[29,30]. Therefore, increasing IFN-γ induction via vaccination is thought to be an important

32

33	strategy for overcoming the tumor progression.

34

35	For vaccine or protein delivery, polymers have mostly been elaborated in the form of

36

37

38	injectable  micro-  or  nano-spheres  or  implant  systems  [31].  The  major  obstacle  of  such

39

40	systems is the complicated fabrication processes using organic solvents, which may cause

41

42

43	denaturation when antigens (or biologically active agents) are to be encapsulated. The use of

44

45	amphiphilic polymers as surfactants differs from those for vaccine delivery and represents a

46

47	new area with significant potential. One example is TiterMax®, wherein a squalene-based

48

49

50	W/O  emulsion  is  stabilized  by  microparticulate  silica  and  non-ionic  block  copolymer

51

52	Pluronic®  [32]. Although TiterMax®  elicits potent immune responses more than emulsified

53

54

55	formulations	based	on	low-molecular	weight	surfactants,	however,	Pluronic®	are

56

57	non-degradable and enhance plasma cholesterol and triglycerol after intraperitoneal injection

58

59

60

61

1	in rat [33]. To meet the above needs, we introduced amphiphilic bioresorbable polymers to

2

3

4	comprise the efficacy and safety of the polymers. We have previously studied the effects of

5

6	bioresorbable polymer-based emulsion on the activation and antigen-presenting functions of

7

8

9	bone  marrow-derived  dendritic  cells  (BMDCs)  [10,23].  Our findings  indicate  that  these

10

11	formulations were biologically inert in BMDCs. In the present study, IVIS data demonstrated

12

13

14	PELA73 provided a depot for bioactive agent CpG at injection site via s.c. administration

15

16	(Fig. 6) and RAH peptide via i.m injection (Fig. S2). With these features in mind, emulsified

17

18	delivery system could serve as either carrier or vehicle to deliver biologically active agents

19

20

21	(e.g. antigens and immunostimulatory adjuvants) to immune cells in a targeted and prolonged

22

23	manner, thus effectively probing and manipulating the vaccine immunogenicity. Concerning

24

25

26	the size of the particles, it is also noteworthy the small solutes or nanoparticles (<50 nm) are

27

28	internalized	by   antigen-presenting	cells	(APCs)	through	macropinocytosis,	whereas

29

30

31	poly(lactide-co-glycolide) microparticles (>500 nm) and oil-in-water emulsion (200 nm in

32

33	size) can be internalized by APCs through phagocytosis without specific recognition has been

34

35	reported	in	the	literature	[34,35].	It	should	be	noted	that	the	dimensions	of

36

37

38	squalane/PEG-PLA/PBS emulsion particles are proper sizes for internalization by APCs to

39

40	facilitate the induction of cell-mediated immunity (Fig. 1). Based on these results, we found

41

42

43	the PEG-PLA-stabilized emulsion have several advantages including proper size for cell

44

45	uptake, stable for long-term storage, and disintegrated post-injection. Scheme 1 represents the

46

47

48	degradation  of  PEG-PLA  and  disintegration  of  PEG-b-PLA-based  squalane  emulsion

49

50	following	immunization.	The	submicron	emulsion	is	stable	during	storage	and

51

52	disintegradable  post-injection.  PEG-PLA-based  emulsion  serves  as  an  antigen  delivery

53

54

55	system  to  favor  the  cell  uptake,  hence  it  triggers  efficient  anti-tumor  immunity  while

56

57	formulated with HPV16 E7(49-57) peptide and CpG immunostimulator. These advances

58

59

60

61

1	open up a new approach to the development of immunotherapy technologies against tumor

2

3

4	challenge.

5

6

7

8

9	4. Conclusions

10

11	Disintegration	characteristics	and	cancer	immunotherapy	potency	of	the

12

13

14	PEG-PLA-emulsified antigen delivery systems were investigated. The results showed that

15

16	squalane/PEG-PLA/PBS	emulsions	are	stable	during	storage	and	disintegratable

17

18	post-injection.   As   adjuvant   for   immunotherapeutic   use,   we   also   demonstrated   that

19

20

21	PEG-PLA-based emulsion is a promising strategy to deliver the designed signals along with

22

23	peptide antigens. Our findings indicated that bioresorbable polymer-emulsified formulations

24

25

26	present great interest as injectable carriers as well as effective inducer to elicit specific T-cell

27

28	response and therapeutic ability in mice. These advances offer the potential in developing

29

30

31	therapeutic cancer vaccine in the future. Further investigations are under way to combine the

32

33	immunotherapy  with  cancer  chemotherapeutic  agents  such  as  paclitaxel  to  prolong  the

34

35	survival of tumor-bearing mice.

36

37

38

39

40	Acknowledgements

41

42

43	This  work  was  supported  by  the  grant  101A1-IVPP24-014  from  National  Health

44

45	Research  Institutes  of  Taiwan,  and  grant  NSC-102-2320-B-400-001-MY2  from  National

46

47

48	Science Council of Taiwan. The authors are grateful to Messrs Chih-Wei Lin and Sheng-Kuo

49

50	Chiang for their help in materials preparedness, and to Dr. Yu-Cheng Chou, Institute of

51

52	Biotechnology  and  Pharmaceutical  Research  of  NHRI  for  his  help  with  the  polymer

53

54

55	characterization.

56

57

58

59

60

61

*References

Click here to download References: 6References_20130907.doc

1	References

2

3

4	[1] Rappuoli R, Dormitzer PR. Influenza: options to improve pandemic preparation. Science

5

6	2012;336:1531-3.

7

8

9	[2] Palucka K, Banchereau J. Cancer immunotherapy via dendritic cells. Nat Rev Cancer

10

11	2012;12:265-77.

12

13

14	[3] Huang RY, Yu YL, Cheng WC, OuYang CN, Fu E, Chu CL. Immunosuppressive effect of

15

16	Quercetin on dendritic cell activation and function. J Immunol 2010;184:6815-21.

17

18	[4]   Song YC, Chou AH, Homhuan A, Huang MH, Chiang SK, Shen KY, et al. Presentation

19

20

21	of lipopeptide by dendritic cells induces anti-tumor responses via an endocytosis-independent

22

23	pathway in vivo. J Leukoc Biol 2011;90:323-32.

24

25

26	[5]   Miconnet I, Coste I, Beermann F, Haeuw JF, Cerottini JC, Bonnefoy JY, et al. Cancer

27

28	vaccine design: a novel bacterial adjuvant for peptide-specific CTL induction. J Immunol

29

30

31	2001;166:4612-9.

32

33	[6]  Shen  SS,  Yang  YW.  Antigen  delivery  for  cross  priming  via  the  emulsion  vaccine

34

35	adjuvants. Vaccine 2012;30:1560-71.

36

37

38	[7]   Aucouturier  J,  Dupuis  L,  Ganne  V.  Adjuvants  designed  for  veterinary  and  human

39

40	vaccines. Vaccine 2001;19:2666-72.

41

42

43	[8]   Seubert  A,  Monaci  E,  Pizza  M,  O'Hagan  DT,  Wack  A.  The  adjuvants  aluminum

44

45	hydroxide  and  MF59  induce  monocyte  and  granulocyte  chemoattractants  and  enhance

46

47

48	monocyte differentiation toward dendritic cells. J Immunol 2008;180:5402-12.

49

50	[9]   Mosca F, Tritto E, Muzzi A, Monaci E, Bagnoli F, Iavarone C, et al. Molecular and

51

52	cellular signatures of human vaccine adjuvants. Proc Natl Acad Sci USA 2008;105:10501-6.

53

54

55	[10] Huang MH, Chou AH, Lien SP, Chen HW, Huang CY, Chen WW, et al. Formulation and

56

57	immunological  evaluation  of  novel  vaccine  delivery  systems  based  on  bioresorbable

58

59

60

61

1	poly(ethylene  glycol)-block-poly(lactide-co-epsilon-caprolactone). J  Biomed Mater Res  B

2

3

4	Appl Biomater 2009;90:832-41.

5

6	[11] Huang MH, Huang CY, Lien SP, Siao SY, Chou AH, Chen HW, et al. Development of

7

8

9	multi-phase  emulsions  based  on  bioresorbable  polymers  and  oily  adjuvant.  Pharm  Res

10

11	2009;26:1856-62.

12

13

14	[12] Huang MH, Huang CY, Lin SC, Chen JH, Ku CC, Chou AH, et al. Enhancement of

15

16	potent  antibody  and  T-cell  responses  by  a  single-dose,  novel  nanoemulsion-formulated

17

18	pandemic influenza vaccine. Microb Infect 2009;11:654-60.

19

20

21	[13] Huang  MH,  Lin  SC,  Hsiao  CH,  Chao  HJ,  Yang  HR,  Liao  CC,  et  al.  Emulsified

22

23	nanoparticles containing inactivated influenza virus and CpG oligodeoxynucleotides critically

24

25

26	influences the host immune responses in mice. PLoS One 2010;5:e12279.

27

28	[14] Babensee JE, Anderson JM, McIntire LV, Mikos AG. Host response to tissue engineered

29

30

31	devices. Adv Drug Del Rev 1998;33:111-39.

32

33	[15] Allison AC. Squalene and squalane emulsions as adjuvants. Methods 1999;19:87-93.

34

35	[16] Salager JL, Loaiza-Maldonado I, Minana-Perez M, Silva F. Surfactant-oil-water systems

36

37

38	near  the  affinity  inversion  part  I:  relationship  between  equilibrium  phase  behavior  and

39

40	emulsion type and stability. J Dispersion Sci Technol 1982;3:279-92.

41

42

43	[17] Clifford GM, Smith JS, Aguado T, Franceschi S. Comparison of HPV type distribution

44

45	in   high-grade   cervical   lesions   and   cervical   cancer:   a   meta-analysis.   Br   J   Cancer

46

47

48	2003;89:101-5.

49

50	[18] Feltkamp MC, Smits HL, Vierboom MP, Minnaar RP, de Jongh BM, Drijfhout JW, et al.

51

52	Vaccination with cytotoxic T lymphocyte epitope-containing peptide protects against a tumor

53

54

55	induced by human papillomavirus type 16-transformed cells. Eur J Immunol 1993;23:2242-9.

56

57	[19] Krieg AM. Therapeutic potential of Toll-like receptor 9 activation. Nat Rev Drug Discov

58

59

60

61

1	2006;5:471-84.

2

3

4	[20] Grizzi  I,  Garreau  H,  Li  S,  Vert  M.  Hydrolytic  degradation  of  devices  based  on

5

6	poly(DL-lactic acid) size-dependence. Biomaterials 1995;16:305-11.

7

8

9	[21] Akagi  T,  Higashi  M,  Kaneko  T,  Kida  T,  Akashi  M.  Hydrolytic  and  enzymatic

10

11	degradation	of	nanoparticles	based	on	amphiphilic	poly(γ-glutamic

12

13

14	acid)-graft-l-phenylalanine copolymers. Biomacromolecules 2006;7:297-303.

15

16	[22] Huang  MH,  Li  S,  Vert  M.  Synthesis  and  degradation  of  PLA–PCL–PLA triblock

17

18	copolymer prepared by successive polymerization of ε-caprolactone and DL-lactide. Polymer

19

20

21	2004;45:8675-81.

22

23	[23] Huang MH, Leng CH, Liu SJ, Chen HW, Sia C, Chong P. Vaccine delivery systems

24

25

26	based on amphiphilic bioresorbable polymers and their role in vaccine immunogenicity. In:

27

28	Villanueva CJ, editor. Immunogenicity. New York: Nova Science Publishers, 2011. p. 61-90.

29

30

31	[24] Reed SG, Bertholet S, Coler RN, Friede M. New horizons in adjuvants for vaccine

32

33	development. Trends Immunol 2009;30:23-32.

34

35	[25] Mbow  ML,  De  Gregorio  E,  Valiante  NM,  Rappuoli  R.  New  adjuvants  for  human

36

37

38	vaccines. Curr Opin Immunol 2010;22:411-6.

39

40	[26] Wheeler CM, Castellsagué X, Garland SM, Szarewski A, Paavonen J, Naud P, et al.

41

42

43	Cross-protective efficacy of HPV-16/18 AS04-adjuvanted vaccine against cervical infection

44

45	and precancer caused by non-vaccine oncogenic HPV types: 4-year end-of-study analysis of

46

47

48	the randomised, double-blind PATRICIA trial. Lancet Oncol 2012;13:100-10.

49

50	[27] Anderson RB, Cianciolo GJ, Kennedy MN, Pizzo SV. α2-Macroglobulin binds CpG

51

52	oligodeoxynucleotides	and	enhances	their	immunostimulatory	properties	by	a

53

54

55	receptor-dependent mechanism. J Leukoc Biol 2008;83:381-92.

56

57	[28] Knutson KL, Disis ML. Tumor antigen-specific T helper cells in cancer immunity and

58

59

60

61

1	immunotherapy. Cancer Immunol Immunother 2005;54:721-8.

2

3

4	[29] Hsu HC, Scott DK, Mountz JD. Impaired apoptosis and immune senescence cause or

5

6	effect? Immunol Rev 2005;205:130-46.

7

8

9	[30] Ikeda H, Chamoto K, Tsuji T, Suzuki Y, Wakita D, Takeshima T, et al. The critical role

10

11	of	type-1	innate	and	acquired	immunity	in	tumor	immunotherapy.	Cancer	Sci

12

13

14	2004;95:697-703.

15

16	[31] O'Hagan D, De Gregorio E. The path to a successful vaccine adjuvant- 'The long and

17

18	winding road'. Drug Discov Today 2009;14:541-51.

19

20

21	[32] Newman MJ, Balusubramanian M, Todd CW. Development of adjuvant-active nonionic

22

23	block copolymers. Adv Drug Del Rev 1998;32:199-223.

24

25

26	[33] Jeong B, Bae YH, Lee DS, Kim SW. Biodegradable block copolymers as injectable

27

28	drug-delivery systems. Nature 1997;388:860-2.

29

30

31	[34] Reddy  ST,  Swartz  MA,  Hubbell  JA.  Targeting  dendritic  cells  with  biomaterials:

32

33	developing the next generation of vaccines. Trends Immunol 2006;27:573-9.

34

35	[35] Seubert A, Calabro S, Santini L, Galli B, Genovese A, Valentini S, et al. Adjuvanticity of

36

37

38	the oil-in-water emulsion MF59 is independent of Nlrp3 inflammasome but requires the

39

40	adaptor protein MyD88. Proc Natl Acad Sci U S A 2011;108:11169-74.

41

42

43

44

45

46

47

48

49

50

51

52

53

54

55

56

57

58

59

60

61

Captions

Click here to download Captions: 7Captions_20130907.doc

Figure captions

Fig. 1. (A) Microscopic aspect and (B) laser light scattering analysis of the emulsified vaccine formulations. Homogeneous fine particles with mean size ranged from 400 to 700 nm were observed in the PELA37-emulsified formulations (blue, left), while 350 to 580 nm were found for the PELA73-emulsified ones (green, right). In the case of PELA55 (orange, middle), a bimodal distribution with two different sizes was observed, the relatively small particles of 450 nm and larger ones of 600 nm. Data are representative for at least five independent experiments.

Fig. 2. Hydrolytic degradation of PEG-PLA and disintegration of PEG-PLA-based squalane emulsion at 37oC. In vitro hydrolytic degradation of PEG-PLA was performed in distilled deionized water at 37°C. Degradation products were recovered by lyophilization and monitored by GPC and MALDI-TOF. (A) Degradation samples were frozen dried then re-dissolved in 1 mL of THF and applied to GPC at 1.0 ml/min flow rate. (B) 1 μL of each sample was applied to form complex with matrix. Dried matrix/analyte complex was used to MALDI-TOF analysis under

reflection mode. Low molecular weight components were measured on a plate containing porous silicone spots without matrix. (C) Visual aspects of the emulsion upon storage at 37oC for six months.

Fig. 3. Hydrolytic degradation of PEG-PLA and disintegration of PEG-PLA-based squalane emulsion at 25oC. In vitro hydrolytic degradation of PEG-PLA was performed in distilled deionized water at 25°C. Degradation products were recovered by lyophilization and monitored by GPC and MALDI-TOF. (A) Degradation samples were frozen dried then re-dissolved in 1 mL of THF and applied to GPC at 1.0 ml/min flow rate. (B) 1 μL of each sample was applied to form complex with matrix. Dried matrix/analyte complex was used to MALDI-TOF analysis under

reflection mode. Low molecular weight components were measured on a plate containing porous silicone spots without matrix. (C) Visual aspects of the emulsion upon storage at 25oC for six months.

Fig. 4. IFN-γ secretion of spleen cells following immunization with RAH peptide antigen. C57BL/6 mice were vaccinated once subcutaneously with 30 µg/dose of RAH peptide, alone or formulated with various adjuvants. Seven days after the immunization, splenocyte suspensions were incubated in the presence or absence of 10

µg/mL of RAH peptide. (A) IFN-γ-producing cells were assessed by ELISPOT assays of cell suspensions for 72 hours of culture. (B) Supernatants collected from triplicate cultures at day 3 were assessed by IFN-γ ELISA. The data are expressed as the mean plus the standard errors of duplicate assays.

Fig. 5. Antitumor efficacy of different adjuvant-formulated RAH peptide on C57BL/6 mice bearing TC-1 tumor cells. (A, B) Mice were inoculated s.c. in the flank with TC-1 tumor cells (2×105 cells/mouse). Upon the appearance of

palpable tumors, eight mice per group were injected s.c. at the tail base with 10 µg/dose of RAH peptide with or without adjuvant on day 7. Tumor sizes were assessed twice per week using calipers to determine the volume of each tumor. The tumor volumes are shown (mm3). (C, D) Mice were inoculated s.c. in the flank with 5×105 TC-1 tumor cells per mouse. On day 7, eight mice per group were injected s.c. at the tail base with 10 µg/dose of RAH peptide with CpG adjuvant or PELA73/CpG combination. Data are expressed as the mean value ± standard deviation. *P<0.05.

Fig. 6. In vivo distribution of (A) RAH-Alexa 647 and (B) CpG-cy5 in mice. C57BL/6 mice were injected s.c. with 10 μg of RAH-Alexa 647 or CpG-cy5 and imaged at 0, 7, 30, 48, 72, and 144 hours after injection by IVIS system.

Scheme 1. Representation of degradation of PEG-PLA and disintegration of PEG-b-PLA-based squalane emulsion following immunization.

Table

Click here to download Table: 8Table1_20130906.doc

Table 1

Physicochemical  characteristics  of  the  emulsified  formulations  comprising  bioresorbable polymer PEG-PLA, phosphate buffer saline, and metabolizable oil squalane

| Acronym | Component |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Oil phase | Water phase |  | O/W (w/w) | Electrolytic conductivity (ms/m) | Particle size (nm) |
| PBS | -- | -- | PBS | -- | 125 | nd |
| Micelles | -- | PEG-PLA | PBS | -- | 135 | 10-15 |
| PELA37 | squalane | PEG-PLA | PBS | 3/7 | 61 | 400-700 |
| PELA55 | squalane | PEG-PLA | PBS | 5/5 | 24 | 400-710 |
| PELA73 | squalane | PEG-PLA | PBS | 7/3 | 12 | 350-580 |
| squalane | squalane | -- | -- | -- | 0 | nd |

nd: non-detectable