Review

Decellularization and Recellularization Technologies in Tissue Engineering

Ru-Huei Fu,*†1,2 Yu-Chi Wang,‡1 Shih-Ping Liu,†§ Ton-Ru Shih,* Hsin-Lien Lin,* Yue-Mi Chen,* Jiun-Huei Sung,* Chia-Hui Lu,* Jing-Rong Wei,* Zih-Wan Wang,* Shyh-Jer Huang,¶ Chang-Hai Tsai,#** Woei-Cherng Shyu,*† and Shinn-Zong Lin*†††‡‡2

*Graduate Institute of Immunology, China Medical University, Taichung 40402, Taiwan

†Center for Neuropsychiatry, China Medical University Hospital, Taichung 40447, Taiwan

‡Biomedical Technology and Device Research Laboratories, Industrial Technology Research Institute, Hsinchu 31040, Taiwan

§Graduate Institute of Basic Medical Science, China Medical University, Taichung 40402, Taiwan

¶Chinese Medicine Research and Development Center, China Medical University Hospital, Taichung 40447, Taiwan

#Department of Pediatrics, China Medical University, Taichung 40402, Taiwan

**Department of Healthcare Administration, Asia University, Taichung 41354, Taiwan

††Deparment of Neurosurgery, China Medical University Beigang Hospital, Yunlin 65152, Taiwan

‡‡Deparment of Neurosurgery, Tainan Municipal An-Nan Hospital-China Medical University, Tainan 70965, Taiwan

1These authors provided equal contribution to this work.

2These authors provided equal contribution to this work.

Address correspondence to Shinn-Zong Lin, M.D., Ph.D., Center for Neuropsychiatry, China Medical University Hospital, No. 2, Yude Road. Taichung 40447, Taiwan. Tel.: +886-4-22052121 ext. 6034; Fax: +886-4-22080666; E-mail: shinnzong@yahoo.com.tw or Ru-Huei Fu, Ph. D., Graduate Institute of Immunology, China Medical University, No. 91, Hsueh-shih Road, Taichung 40402, Taiwan. Tel.: +886-4-22052121 ext. 7826; Fax: +886-4-22052121 ext. 7810; E-mail: rhfu@mail.cmu.edu.tw

Running head: Decellularization Technology in Tissue Engineering

ABSTRACT

Decellularization is the process by which cells are discharged from tissues/organs, but all of the necessary cues for cell maintenance and homeostasis are retained in a three-dimensional structure of the organ and its extracellular matrix components. During tissue decellularization, preservation of the native ultrastructure and composition of the extracellular matrix (ECM) is highly desirable. For recellularization, the scaffold/matrix is seeded with cells, the final goal being to form a functional organ. In this review, we focus on the biological properties of the ECM that remains when various decellularization methods are used; compare recellularization technologies, including bioreactor development for perfusion-based bioartificial organs; and discuss cell sources. In future, such a process may solve the problem of organ assembly on demand.

Key words: Biomaterial; Decellularization; Extracellular matrix; Organ bioengineering and regeneration; Recellularization

Introduction

Tissue engineering approaches have thus far been able to partially enhance cell engraftment by improving cells and cell contact in animal models and by supplying nonimmunogenic matrices before transplantation (45). However, these methods are limited to transplantation into less vascularized areas and two-dimensional structures (58,61,95). Promising clinical tests involve the use of two main scaffolds: synthesized material and a natural matrix (6,59). Synthetic scaffolds are made of polymers such as polypropylene or polyglycolic acid. Decellularized natural matrices are another source of material for the scaffold. The use of decellularized scaffolds is an attractive technique because the resulting material is likely to preserve the original architecture of the tissue or organ, including the function of native microvascular systems (4).

A review of tissue decellularization techniques and developments was published in 2006 (28), but new developments in these techniques using three-dimensional whole organ decellularization have since emerged (17). The purpose of the present review is to focus on the biological properties of the extracellular matrix (ECM) that remains when various decellularization methods are used, after which stem or progenitor cells are seeded on the biological scaffold with ECM proteins and the cells are expected to proliferate and differentiate, as well as to compare recellularization technologies.

Decellularization and Recellularization Technologies

The objective of the decellularization protocol is to minimize any adverse effect on the composition, biological activity, and mechanical integrity of the remaining ECM after efficiently removing all cellular and nuclear materials (Figure 1). Any processing step intended to remove cells during decellularization will change the native three-dimensional architecture of the ECM. The challenge in decellularization is to find the optimal protocols that will retain the native ECM for clinical use, depending on its intended purpose.

The most commonly used methods for the decellularization of tissues involve a combination of chemical, enzymatic, and physical approaches. Various procedures have been developed to eliminate the cellular component of both native and engineered tissues while minimally disrupting the ECM. Decellularization protocols typically began with lysing the cell membrane by using physical treatments or ionic solutions, and then separating the cellular components from the ECM by using enzymatic treatments and detergents for the solubilization of cytoplasmic and nuclear cellular components, and finally removing cellular debris from the tissue. These steps can be done with mechanical agitation to enhance their effectiveness. To avoid an adverse host-tissue response to the chemicals, all residual chemicals must be removed after decellularization. According to the report of Crapo et al., DNA content needs to be less than 50 ng/mg tissue for sufficient decellularization (17).

The detailed methods described in the literature combine several of these principal techniques in order to increase the efficiency of decellularization and, at the same time, to reduce the potential damage to the ECM by exposing it to less destructive conditions.

Chemical compounds

Acids and bases (69) work to denature proteins, solubilize cell components, and alter nucleic acids, thus rupturing the cells. Because they are not selective, however, they alter the ECM components, especially collagen, glycosaminoglycan (GAG), and growth factors.

Hypertonic and hypotonic solutions (99) disrupt cells through osmotic shock and also interfere with the interaction between DNA and proteins. Although being relatively efficient at disrupting cells, they do a poor job of removing cellular residues.

Ionic or non-ionic detergents, or a combination of both (79), destroy DNA-protein interactions, lipids, and lipoproteins, and may denature proteins. As a result of their action on cells, they also damage the ECM ultrastructure, leading to a loss of collagens, growth factors, and GAG.

Other solvents such as alcohol and glycerol aid in dehydrating and lysing cells during tissue decellularization (67). Acetone can also be used to remove lipids during decellularization (49,54). However, like alcohols, acetone is a tissue fixative (40) and damages the ECM ultrastructure (15), warranting conservative use, especially for biological scaffolds used in load-bearing clinical applications (30, 31). Tributyl phosphate (TBP) is an organic solvent with viricidal properties. For decellularization of dense tissues such as tendons, TBP is more effective than detergents such as Triton X-100 and SDS, with varying effects on the retention of ECM constituents and its native mechanical properties (21, 13).

Biologic solutions

Enzymes (66) can be used to target the remnant nucleic acids after cell rupture or to target the peptide bonds that anchor the cells to the ECM. They tend to remain in the tissue in significant quantities and may lead to higher levels of immune response. Long-term exposure can also result in the removal of collagens, laminin, fibronectin, elastin, and GAG, as well as damage to the ECM ultrastructure.

Non-enzymatic agents—chelating agents such as ethylenediaminetetraacetic acid (EDTA) and ethylene glycol tetraacetic acid—have a particular way of binding with ions and metal ions that helps cells to dissociate from ECM proteins by sequestering metal ions (43, 27).

Other agents: physical and miscellaneous

Pressure, temperature, force, and nonthermal irreversible electroporation (NTIRE) can also be used in decellularization protocols. Multiple freeze-thaw cycles may be used (16) that do not significantly increase the loss of ECM proteins from tissue (65). Cells on the surface of a tissue or organ such as urinary bladder, small intestine, skin, and amnion can be effectively removed by mechanical abrasion in combination with enzymes (36), hypertonic saline, or chelating agents, all of which facilitate dissociation of cells from their subjacent basement membrane. NTIRE has also been investigated as an approach to tissue decellularization (74).

The optimal conditions for decellularization agents are dependent on tissue characteristics such as thickness and density, the agents being used, and the expected clinical application of the decellularized tissue. Before decellularization agents are applied, any undesirable excess tissue may be removed to simplify the cell removal process (26). Still, some problems remain common to all agents. First, all existing techniques rely on cell lysis. The resulting cell debris can thus freely adsorb to the remaining matrix, consequently increasing immunogenicity, leading to contradictory results (8). Second, existing techniques have been proven to degrade some components of the ECM (17). On the other hand, pathogenic viruses that place the recipient at considerable risk are thought to be eliminated by endonuclease treatment, as integrated viral DNA/RNA is likewise fragmented. Maintenance of the native tissue architecture, ECM components, and growth factors for proper cellular homing and differentiation are the important properties of these scaffolds. The autologous or allogeneic cells are seeded back into the scaffolds to repopulate the matrix and return function to the organ. Several methods are used to reseed scaffolds, with dynamic cell seeding methods tending to be more effective than static methods (92, 96). To date, static seeding is the most common method in the construction of tissue, in which a concentrated cell suspension is passively introduced to a scaffold. This seeding technique yields seeding efficiencies of approximately 10%–25% (3). This technique has several limitations, however, such as low seeding efficiency and minimal cell penetration of scaffold walls. To overcome some of these drawbacks, alternate seeding techniques have been developed, including magnetic, dynamic, electrostatic, vacuum, and centrifugal seeding (92). The most common of the dynamic methods for reseeding is to directly add cells at high concentration into the vascular perfusion line just upstream of the organ, allowing cells to travel directly through the vascular tree into the scaffold and parenchyma. This method is widely used in recellularization (64) of the blood vessels of the heart, lung (63), and liver (7, 85). Many researchers have delivered cells through the scaffold vasculature to an organ parenchyma, and the cells are thought to traverse the vascular lining through holes or pores created by the decellularization process. During this reseeding process, low flow rates are used to reduce the shear stress on the cells. For the liver, a high seeding efficiency (86%–96%) has been reported by directly injecting into the portal vein through the bioreactor inlet port; dividing the cells into multiple injections is superior to a single infusion with the same total number of cells (85, 91).

Portal vein-seeded endothelial cells were reported to be primarily deposited in the periportal regions of the liver lobule, while the vena cava-seeded endothelial cells were primarily concentrated in the regions of the central veins and in smaller branches and vessels (11). The second way to recellularize the liver is to inoculate cells into the bulk media and allow them to recycle through the circuit to reseed the organ; however, this achieved a lower seeding efficiency (69%) than did the method described earlier (85).

The organ parenchyma cells may be seeded together in a mixture (7, 63) with endothelial cells or via separate inoculations of pure cell populations (85, 91). Using a small gauge needle, direct inoculation of cells into several locations of organ parenchyma is an alternative method of recellularization (64, 78). However, this method was less efficient than delivering hepatocytes through the vasculature (85). Although the vascular system is most commonly used to introduce cells into a scaffold, other routes may be needed to populate the diverse cell types that make up an organ. The lung is the most developed model for alternative delivery of specialized cells, with the tracheobronchial tree primarily used to deliver pneumocytes or mesenchymal stem cells (10). Delivery of specialized cells such as urothelium to growing kidneys and cholangiocytes to the liver will likely require direct seeding through the ureter or bile duct, respectively.

A cylindrical configuration and spinner flask are available in bioreactors used for cell seeding. Bioreactors have both advantages and disadvantages. The cylindrical configuration limits dead zones and promotes mixing, as determined by mathematical modeling and experimentation (46). An often-used bioreactor design is a spinner flask with a stir bar on the bottom, which is especially useful when seeding cells into bulk media. The continuous-flow stirred tank reactor keeps cells in suspension that may have failed to lodge in the scaffold during a pass through the bioreactor, allowing for multiple passes through the scaffold. However, the cells used in recellularizing an organ are adhesion-dependent, and so anoikis may occur if cells recirculate for extended periods. The organ is typically suspended on the inlet line, and stirring the bulk fluid may lead to adverse rotational shear on the organ. Suspending the stir bar will minimize lysis of cells caught between the vessel and the stir bar (71). During organ decellularization, flow resistance is reduced because the scaffold is inversely proportional to cell density and porosity (55). But as reseeded cells flow into the vascular tree, pores will fill with cells and the pressure drop will increase as the porosity decreases (46). During reseeding, increasing the cell seeding density increases the possibility of cell aggregates occluding vessels and forming thick polylayers. This can result in oxygen and nutrients becoming mass transfer limited, leading to hypoxia and the development of a necrotic core (39,42,52,98). Experimentation to determine the optimal media content is critical. The addition of extra growth factors may be necessary if sufficient levels are not retained in the ECM. However, it is important to maintain an appropriate balance. For example, vascular endothelial growth factor (VEGF) is required for endothelial cells to seed the scaffold vasculature and to form new vessels. But when high levels of VEGF and fibroblast growth factor (FGF) are added, giant cells and aggregates form (93). At times, modification of the oxygen level is needed.

The bioreactor may need to provide the growing organ with physical, electrical, or chemical stimulation, or a combination of these, depending on the situation. For example, the heart needs to be mechanically stretched and electrically stimulated. Mechanically stretching tissue promotes cell alignment, elongation, and expression of connexin-43, a cardiac marker (51). Electrical stimulation can also be used in tandem with mechanical stretching (51,88). The lung requires special consideration for the bioreactor design. As the lung is inflated and deflated, the ECM must retain appropriate mechanical compliance. In order to achieve this, the common method used in a bioreactor is to suspend the lung scaffold in a container of media and to connect the lungs to a ventilator that matches the volume and respiratory rate of the animal (53,68,81,82). In a lung transplanted from a rat, with the bioreactor design, it is possible to recellularize the cadaveric lung to such an extent that improvement in oxygen exchange can be demonstrated with the recellularized lung at seven days (81, 82). The kidney does not require mechanical stimulation, but benefits from chemical stimulation. Humes et al. found that when kidneys were cultured with transforming growth factor 1 and trans-retinoic acid, renal proximal tubule cells grew as a monolayer and formed lumens with polarized epithelial layers, microvilli, and tight junction complexes; this did not occur without these factors (37). After culturing, the cells were incorporated into hollow fibers and connected through an extracorporeal circuit to dogs with renal failure. The hollow fibers containing proximal tubule cells increased the level of activated vitamin D (1,25–dihydroxy: vitamin D3) by 5.8 pmol/ml from the uremic dog’s pretreatment baseline over the course of three days, whereas activated vitamin D levels in dogs with sham-control hollow fibers decreased by 4.0 pmol/ml from their pretreatment level (24).

Tissue decellularization might be applicable to any organ. The construction of perfusion-decellularized native ECM scaffolds that match organs in size and structure is the first step toward generating functional tissue that can be transplanted. However, they require improvement and customization in size, category, species, and cell sources. More important, the resulting scaffolds need to be reproducible, sterile, and preservable for future procedures.

The ECM

For every tissue and organ in the body, the ECM is a combination of structural and functional proteins, lipids, proteoglycans, and crystals that has a unique composition and physical properties. The ECM has been shown to specifically promote cell aggregation, adhesion, migration, proliferation, and differentiation in a way that reflects the functional requirements and biological identity of tissues (17). Such guiding elements may be retained, at least in part, even in the absence of living cellular components. On the basis of this rationale, the decellularized ECM has received more and more attention in the field of regenerative medicine as an off-the- shelf and immune-compatible alternative to living grafts for tissue and organ repair (Fig. 1). Decellularized ECM is expected to induce regenerative processes, not only through specific “organomorphic” structures (89), but also by its physiological presentation. The ECM is involved in cell communication, as well as in defining the shape and stability of tissues (83). The instructive scaffold materials derived from decellularized ECM could be activated by living cells prior to implantation, with the assumption that the ECM is capable of directing the differentiation fate of the seeded cells (20,22,41,73). During the process of tissue decellularization, preservation of the native ultrastructure and composition of the ECM is highly desirable (2,5,60,64,66,80,91). The efficiency of decellularization and the preservation of the ECM can be evaluated through a variety of methods. Some commonly used agents (e.g., chemical, enzymatic, and physical) and their effects on cellular and extracellular tissue constituents are reviewed in the following sections (17).

Chemical compounds

Alkaline and acid treatments are used to solubilize the cellular components dissolved in the cytoplasm, as well as to remove nucleic acids such as RNA and DNA. For example, acetic acid, peracetic acid (PAA), hydrochloric acid, sulfuric acid, and ammonium hydroxide can effectively disrupt cell membranes and intracellular organelles in decellularization protocols (19,23,25). Unfortunately, these chemicals also dissociate important molecules such as GAGs from collagenous tissues. In porcine urinary bladder, for example, the concentration of PAA at about 0.10-0.15 (w/v) is highly efficient at removing cellular material (47), and the effect of PAA treatment on ECM components has been studied extensively. However, the microstructure of the collagen fibers is not the same as before treatment (12). Like hyaluronic acid, heparin, heparin sulfate, chondroitin sulfate A, and dermatan sulfate retain many of the native GAGs following PAA treatment (34). PAA treatment retains the structure and function of many of the growth factors that are resident in the ECM, including transforming growth factor , basic fibroblast growth factor (FGF), and vascular endothelial growth factor (VEGF) (35,94).

Non-ionic detergents destroy lipid–lipid and lipid–protein interactions, but leave protein– protein interactions intact; thus, proteins within a tissue or organ should be left in a functional conformation under non-ionic detergent treatment (77). Triton X-100 is the most widely studied non-ionic detergent for decellularization protocols. In valve tissue, Triton X-100 led to a nearly complete loss of GAGs and decreased the laminin and fibronectin content of the valve tissue (32). The most commonly used ionic detergent is sodium dodecyl sulfate (SDS) (70). Compared with other detergents, SDS yields more complete removal of nuclear remnants and cytoplasmic proteins, such as vimentin. SDS tends to destroy the native tissue structure, however, and to result in reduced concentrations of GAG and loss of collagen integrity (97).

TBP treatment did not have an effect on the tensile strength of collagen fibers isolated from rat tail tendon, as compared with the native control, but it did on the anterior cruciate ligament, resulting in a decrease in collagen content (97) after TBP treatment. TBP appears to be a promising chaotropic agent that has minimal impact on the mechanical behavior of the ECM and is worthy of further study (21).

Biologic solutions

Trypsin is one of the most commonly used proteolytic enzymes in subculture for passaging cells. However, enzymatic methods of decellularization are not without adverse effects on the extracellular components of tissues and organs. Long-term treatment with trypsin/EDTA was reported to result in disruption of the normal pulmonary valve ECM structure, but did not affect the amount of collagen in the tissue (76). Prolonged exposure to trypsin/EDTA significantly reduced the elastin content and GAGs over time, with o-sulfated GAGs (chondroitin sulfates, keratin sulfates, and dermatan sulfates) showing the greatest decrease. Such treatments can reduce tensile strength by up to 50%.

The ECM that remains after such enzymatic decellularization protocols still supports endothelial cell growth in vitro despite the removal of ECM components (32,76). It is nonetheless desirable to limit exposure to trypsin/EDTA treatment to minimize the disruptive effects on the ultrastructure and composition of the ECM.

Other agents: physical and miscellaneous

The temperature must be carefully controlled to prevent the formation of ice, as well as to interrupt the rate of change of the ECM. Although freezing can be an effective method of cell lysis, it must be followed by processes to remove the cellular material from the tissue (48). Even when the number of cycles was increased to 10, freeze-thaw cycling alone could not remove all of the cell nuclei (48). However, freeze-thaw cycling combined with other methods can be used to achieve more successful decellularization. According to some reports, freeze-thaw cycling can be combined with detergent and nucleases to achieve optimal decellularization of menisci (86). It has also been reported that cellular components can be removed by freeze-thaw cycling and ammonium hydroxide, while retaining the ECM in two-dimensional culture systems (33).

Cells can be lysed by applying direct pressure to tissue, but this method is effective only for tissues or organs that are not characterized by densely organized ECM (e.g., liver, lung). Organs such as the small intestine (62) and (72) bladder are characterized by natural planes of dissection in which mechanical force can be used to delaminate the tissue layers from these organs.

These methods are effective, causing minimal disruption to the three-dimensional architecture of the ECM within these tissues. In the present review, we have evaluated the effect of the most commonly used chemical and physical decellularization methods on the ECM in order to optimize a decellularization method for future studies. Further studies are necessary to improve the preparation processes and to optimize the methods of applying ECM scaffolds for tissue regeneration.

Cells for Recellularization

The clinical quality and scale of the scaffolds is only the first step of many toward the regeneration of viable and functional organs. At the current stage of technology, an attempt to recapitulate the entire process of embryogenesis from the single cell stage to organogenesis in the laboratory setting seems unrealistic. The ideal clinically viable progenitor population as a source of cells has not yet been identified. Embryonic stem cells (ES cells) carry ethical and supply issues and are immunogenic, thus affecting their clinical value. Induced pluripotent stem cells derived from adult cells are an alternative, although disease-related mutations might need to be corrected (e.g., BMPR2 mutations in pulmonary hypertension) and concerns surrounding genetic alterations may need to be resolved. Creating differentiated cell numbers required for the regeneration of human-sized organs exceeds current progenitor cell technology and poses significant challenges in phenotypic control at a large scale (56).

Different cell sources, including pig cells, fetal cells, induced pluripotent stem cells (87), and ES cells (44), are currently available, or being investigated as a new paradigm for future therapies of many intractable diseases. The use of stem cells in several clinical trials has begun, although the results are controversial (1,9,90). Cells are engineered and multiplied in culture before transplantation, or after use with minimal manipulation after harvesting or isolation, and then delivered directly or by using bioengineering strategies. The transplanted cells are expected to home to the site of interest (e.g., the liver) or to remain at the injection site, depending on the particular application. The main challenge in this area is to transition rapidly from the identification of candidate cell populations to the development of effective delivery approaches.

Xenogeneic cells may also be a potential source of cells that could solve many of the challenges in treating organ failure. The xenotransplantation of cells is not limited by the availability of donors, could be performed repeatedly if needed, and may be effective for the treatment of viral disease (100,63). The most difficult obstacle to xenotransplantation is the immunological rejection of organ transplantation, but major efforts are ongoing to elucidate the exact mechanism involved in cell rejection. Previous studies showed that porcine hepatocytes survive immune suppression for up to 3 months after injection in monkey spleen, thus indicating that xenotransplantation of pig hepatocytes into patients with severe liver failure (57,35) may become an option in the future.

These studies show that the effectiveness of decellularization and the alterations to the ECM vary, depending on the source of the tissue, its composition, its density, and other factors (28). Recently, because of the progress in guiding cell differentiation toward specific lineages, in vitro engineered tissues are also being considered as a substrate for decellularization. This approach opens the possibility of generating large quantities of standardized, customized grafts.

The potential applications of decellularized matrix in tissue engineering have been demonstrated for a number of tissues, including liver (11, 91), kidney (60), pancreas (29), bladder (99), artery, esophagus (18), skin (75), and trachea (50). More recently, another group reported the decellularization of an entire heart through perfusion, preserving the original architecture and original microvascular network and allowing for extensive recellularization (64).

Future Prospects

We have reviewed the latest technology in regenerative therapies necessitating whole organ decellularization and the effectiveness of the application. Many of the current efforts aimed at developing strategies for expansion and stemness (e.g., fibroblast reprogramming that skips pluripotent progenitor stages (38) and ES cell-derived protein-induced pluripotency (14)) might deliver novel solutions applicable to organ engineering in the foreseeable future. Compared with the successful clinical application of this technology in skin or vessels, which was established early on, there is a great need to overcome many functional and structural issues before it can be used for organ replacement. This method has currently achieved only short-term functionality in vivo and then only in rodent models. Work in tissue engineering in recent decades, and currently work in the field of stem cell research, is producing encouraging results, which some day might solve the problem of organ assembly on demand (84). Solid organ regeneration based on perfusion-decellularized native ECM scaffolds has a huge potential in patients with organ failure, one that is apparently still an ambitious goal.

ACKNOWLEDGMENTS: This work was supported by the National Science Council (Taiwan) (NSC 100-2314-B-039-036), the Taiwan Department of Health Clinical Trial and Research Center of Excellence (DOH102-TD-B-111-004), and China Medical University (DMR103-054). The authors declare no conflict of interest.

REFERENCES

1.	Abdel-Latif, A. B. R.; Tleyjeh, I. M.; Montori, V. M.; Perin, E. C.; Hornung, C. A.; Zuba-Surma, E. K.; Al-Mallah, M.; Dawn, B. Adult bone marrow-derived cells for cardiac repair: a systematic review and meta-analysis. Arch. Intern. Med. 167:989-997; 2007.

2.	Allen, R. A.; Seltz, L. M.; Jiang, H.; Kasick, R. T.; Sellaro, T. L.; Badylak, S. F.; Ogilvie, J. B. Adrenal extracellular matrix scaffolds support adrenocortical cell proliferation and function in vitro. Tissue Eng. Part A 16:3363-3374; 2010.

3.	Aunins, J. G.; Woodson, B. A.; Hale, T. K.; Wang, D. I. Effects of paddleimpeller geometry on power input and mass transfer in small-scale animal cell culture vessels . Biotech. Bioeng. 34:1127-1132; 1989.

4.	Badylak, S. F. The extracellular matrix as a biologic scaffold material. Biomaterials 28:3587-3593; 2007.

5.	Badylak, S. F.; Freytes, D. O.; Gilbert, T. W. Extracellular matrix as a biological scaffold material: Structure and function. Acta Biomater. 5:1-13; 2009.

6.	Baiguera S, B. M., Macchiarini P. Tissue-engineered tracheal transplantation. Transplantation 89:485-491; 2010.

7.	Baptista, P. M.; Siddiqui, M. M.; Lozier, G.; Rodriguez, S. R.; Atala, A.; Soker; S. The use of whole organ decellularization for the generation of a vascularized liver organoid. Hepatology 53:604-617; 2011.

8.	Boer, U.; Lohrenz, A.; Klingenberg, M.; Pich, A.; Haverich, A.; Wilhelmi, M. The effect of detergent-based decellularization procedures on cellular proteins and immunogenicity in equine carotid artery grafts. Biomaterials 32:9730-9737; 2011.

9.	Bolli, R. C. A.; D'Amario, D.; Loughran, J.H.; Stoddard, M.F.; Ikram, S.; Beache, G.M.; Wagner, S. G.; Leri, A.; Hosoda, T.; Sanada, F.; Elmore, J. B.; Goichberg, P.; Cappetta, D.; Solankhi, N.K.; Fahsah, I.; Rokosh, D. G.; Slaughter, M. S.; Kajstura, J.; Anversa, P. Cardiac stem cells in patients with ischaemic cardiomyopathy (SCIPIO): initial results of a randomised phase 1 trial. Lancet 378:1847-1857; 2011.

10.	Bonvillain, R. W.; Danchuk, S.; Sullivan, D. E.; Betancourt, A. M.; Semon, J. A.; Eagle, M. E.; Mayeux, J. P.; Gregory, A. N.; Wang, G.; Townley, I. K.; Borg, Z. D,; Weiss, D. J.; Bunnell, B. A. A nonhuman primate model of lung regeneration: detergent-mediated decellularization and initial in vitro recellularization with mesenchymal stem cells. Tissue Eng. Part A 18:2437-2452; 2012.

11.	Booth, C.; Soker, T.; Baptista, P.; Ross, C.L.; Soker, S.; Farooq, U.; Stratta, R.J.; Orlando, G. Liver bioengineering: current status and future perspectives. World J. Gastroenterol. 18:6926-6934; 2012.

12.	Brown, B.; Lindberg, K.; Reing, J.; Stolz, D. B.; Badylak, S. F. The basement membrane component of biologic scaffolds derived from extracellular matrix. Tissue Eng. 12:519-526; 2006.

13.	Cartmell, J. S.; Dunn M. G. Effect of chemical treatments on tendon cellularity and mechanical properties. J. Biomed. Mater. Res. 49:134-140; 2000.

14.	Cho, H. J.; Lee C. S.; Kwon, Y. W.; Paek, J. S.; Lee, S.H.; Hur, J.; Lee, E. J.; Roh, T. Y.; Chu, I. S.; Leem; S. H.; Kim, Y.; Kang, H. J.; Park, Y. B.; Kim, H. S. Induction of pluripotent stem cells from adult somatic cells by protein-based reprogramming without genetic manipulation. Blood 116:386-395; 2010.

15.	Cole, M. B. Jr. Alteration of cartilage matrix morphology with histological processing. J. Microsc. 133:129-140; 1984.

16.	Cortiella, J.; Niles, J.; Cantu, A.; Brettler, A.; Pham, A.; Vargas, G.; Winston, S.; Wang, J.; Walls, S.; Nichols, J. E. Influence of acellular natural lung matrix on murine embryonic stem cell differentiation and tissue formation. Tissue Eng. Part A 16:2565-2580; 2010.

17.	Crapo, P. M.; Gilbert T.W.; Badylak, S.F. An overview of tissue and whole organ decellularization processes. Biomaterials 32:3233-3243; 2011.

18.	Dahl, S. L.; Koh, J.; Prabhakar, V.; Niklason, L. E. Decellularized native and engineered arterial scaffolds for transplantation. Cell Transplant. 12:659-666; 2003.

19.	De Filippo, R. E.; Yoo, J.; Atala, A. Urethral replacement using cell seeded tubularized collagen matrices. J. Urol. 168:1789-1792; 2002.

20.	Decaris, M. L.; Binder B.Y.; Soicher, M. A.; Bhat, A.; Leach, J. K. Cell-derived matrix coatings for polymeric scaffolds. Tissue Eng. Part A 18:2148-2157; 2012.

21.	Deeken, C. R.; White, A. K.; Bachman, S. L.; Ramshaw, B. J.; Cleveland, D. S.; Loy, T. S.; Grant, S. A. Method of preparing a decellularized porcine tendon using tributyl phosphate. J. Biomed. Mater. Res. B Appl. Biomater. 96:199-206; 2011.

22.	Evan, G.. Getting one’s Fak straight. Dev. Cell 19:185-186; 2010.

23.	Falke, G.; Yoo, J.; Kwon, T. G.; Moreland, R.; Atala, A. Formation of corporal tissue architecture in vivo using human cavernosal muscle and endothelial cells seeded on collagen matrices. Tissue Eng. Part A 9:871-879; 2003.

24.	Fissell, W. H.; Kimball, J.; MacKay, S. M.; Funke, A.; Humes, H. D. The role of a bioengineered artificial kidney in renal failure. Ann. N. Y. Acad. Sci. 944:284-295; 2001.

25.	Freytes, D. O.; Badylak S. F.; Webster, T. J.; Geddes, L. A.; Rundell, A. E. Biaxial strength of multilaminated extracellular matrix scaffolds. Biomaterials 25:2353-2361; 2004.

26.	Freytes, D. O.; Stoner, R. M.; Badylak, S. F. Uniaxial and biaxial properties of terminally sterilized porcine urinary bladder matrix scaffolds. J. Biomed. Mater. Res. B Appl. Biomater. 84:408-414; 2008.

27.	Gailit, J.; Ruoslahti, E. Regulation of the fibronectin receptor affinity by divalent cations. J. Biol. Chem. 263:12927-12932; 1988.

28.	Gilbert, T. W.; Sellaro, T. L.; Badylak, S. F. Decellularization of tissues and organs. Biomaterials 27:3675-3683; 2006.

29.	Goh, S. K.; Bertera, S.; Olsen, P.; Candiello, J. E.; Halfter, W.; Uechi, G.; Balasubramani, M.; Johnson, S. A.; Sicari, B. M.; Kollar, E.; Badylak, S. F.; Banerjee, I. Perfusion-decellularized pancreas as a natural 3D scaffold for pancreatic tissue and whole organ engineering. Biomaterials 34:6760-6772; 2013.

30.	Gorschewsky, O. K. A.; Riechert, K.; Pitzl, M.; Becker, R. Clinical comparison of the Tutoplast allograft and autologous patellar tendon (bone-patellar tendon-bone) for the reconstruction of the anterior cruciate ligament: 2- and 6-year results. Am. J. Sports Med. 33:1202-1209; 2005.

31.	Gorschewsky, O.; Puetz A.; Riechert, K.; Klakow, A.; Becker, R. Quantitative analysis of biochemical characteristics of bone-patellar tendon-bone allografts. Biomed. Mater. Eng. 15:403-411; 2005.

32.	Grauss, R. W.; Hazekamp, M. G.; Oppenhuizen, F.; van Munsteren, C. J.; Gittenberger-de Groot, A. C.; DeRuiter, M. C. Histological evaluation of decellularised porcine aortic valves: matrix changes due to different decellularisation methods. Eur. J. Cardiothorac. Surg. 27:566-571; 2005.

33.	Ho, T. C.; Del Priore L. V. Reattachment of cultured human retinal pigment epithelium to extracellular matrix and human Bruch’s membrane. Invest. Ophthalmol. Vis. Sci. 38:1110-1118; 1997.

34.	Hodde, J. P.; Badylak S. F.; Brightman, A. O.; Voytik-Harbin, S. L. Glycosaminoglycan content of small intestinal submucosa: a bioscaffold for tissue replacement. Tissue Eng. Park A 2:209-217; 1996.

35.	Hodde, J. P.; Record, R. D.; Liang, H. A.; Badylak, S. F. Vascular endothelial growth factor in porcine-derived extracellular matrix. Endothelium 8:11-24; 2001.

36.	Hopkinson, A. S. V.; Gray, T.; Yeung, A. M.; Lowe, J.; James, D. K.; Dua, H. S. Optimization of amniotic membrane (AM) denuding for tissue engineering. Tissue Eng. Part C Methods 14:371-381; 2008.

37.	Humes, H. D.; Cieslinski, D. A. Interaction between growth factors and retinoic acid in the induction of kidneytubulogenesis in tissue culture. Exp. Cell Res. 201:8-15; 1992.

38.	Ieda, M. F. J., Delgado-Olguin, P.; Vedantham, V.; Hayashi, Y.; Bruneau, B. G.; Srivastava, D. Direct reprogramming of fibroblasts into functional cardiomyocytes by defined factors. Cell 142:375-386; 2010.

39.	Issa, R. I.; Engebretson, B.; Rustom, L.; McFetridge, P. S.; Sikavitsas, V. I. The effect of cell seeding density on the cellular and mechanical properties of a mechanostimulated tissueengineered tendon. Tissue Eng. Part A 17:1479-1487; 2011.

40.	Jamur, M. C.; Oliver, C. Cell fixatives for immunostaining. Methods Mol. Biol. 588:55-61; 2010.

41.	Kang, Y.; Kim S.; Bishop, J.; Khademhosseini, A.; Yang, Y. The osteogenic differentiation of human bone marrow MSCs on HUVEC-derived ECM and beta-TCP scaffold. Biomaterials 33:6998-7007; 2012.

42.	Kim, K.; Dean D.; Lu, A.; Mikos, A. G.; Fisher, J. P. Early osteogenic signal expression of rat bone marrow stromal cells is influenced by both hydroxyapatite nanoparticle content and initial cell seeding density in biodegradable nanocomposite scaffolds. Acta Biomater. 7:1249-1264; 2011.

43.	Klebe, R. J. Isolation of a collagen-dependent cell attachment factor. Nature 250:248-251; 1974.

44.	Kriks, S.; Shim, J. W.; Piao, J.; Ganat, Y. M.; Wakeman, D. R.; Xie, Z.; Carrillo-Reid, L.; Auyeung, G.; Antonacci, C.; Buch, A.; Yang, L.; Beal, M. F.; Surmeier, D. J.; Kordower, J. H; Tabar, V.; Studer, L. Dopamine neurons derived from human ES cells efficiently engraft in animal models of Parkinson's disease. Nature 480:547-551; 2011

45.	Langer, R.; Vacanti, J. P. Tissue engineering. Science 260:920-926; 1993.

46.	Lawrence, B. J.; Devarapalli, M.; Madihally, S. V. Flow dynamics in bioreactors containing tissue engineering scaffolds. Biotech. Bioeng. 102:935-947; 2008.

47.	Liu, Y.; Bharadwai, S.; Lee, S. J.; Atala, A.; Zhang, Y. Optimization of a natural collagen scaffold to aid cell-matrix penetration for urologic tissue engineering. Biomaterials 30:3865-3873; 2009.

48.	Lu, H.; Hoshiba, T.; Kawazoe, N.; Chen, G. Comparison of decellularization techniques for preparation of extracellular matrix scaffolds derived from three-dimensional cell culture. J. Biomed. Mater. Res. A 100:2507-2516; 2012

49.	Lumpkins, S. B.; Pierre, N.; McFetridge, P. S. A mechanical evaluation of three decellularization methods in the design of a xenogeneic scaffold for tissue engineering the temporomandibular joint disc. Acta Biomater. 4:808-816; 2008.

50.	Macchiarini P, J. P.; Go, T.; Asnaghi, M.A.; Rees, L. E.; Cogan, T. A.; Dodson, A.; Martorell, J.; Bellini, S.; Parnigotto, P. P.; Dickinson, S. C.; Hollander, A. P.; Mantero, S.; Conconi, M. T.; Birchall, M. A. Clinical transplantation of a tissue-engineered airway. Lancet 372:2023-2030; 2008.

51.	Maidhof, R.; Tandon, N.; Lee, E. J.; Luo, J.; Duan, Y.; Yeager, K.; Konofagou, E.; Vunjak-novakovic, G. Biomimetic perfusion and electrical stimulation applied in concert improved the assembly of engineered cardiac tissue. J. Tissue Eng. Regen. Med. 6:e12-e23; 2012.

52.	Melchels F. P.; Tonnarelli, B.; Olivares, A. L.; Martin, I.; Lacroix, D.; Feijen, J.; Wendt, D. J.; Grijpma, D. W. The influence of the scaffold design on the distribution of adhering cells after perfusion cell seeding. Biomaterials 32:2878-2884; 2011.

53.	Mishra, D. K.; Thrall, M. J.; Baird, B. N.; Ott, H. C.; Blackmon, S. H.; Kurie, J. M.; Kim M. P. Human lung cancer cells grown on acellular rat lung matrix create perfusable tumor nodules. Ann. Thorac. Surg. 93:1075-1081; 2012.

54.	Montoya, C. V.; McGetridge P. S. Preparation of ex vivo-based biomaterials using convective flow decellularization. Tissue Eng. Part C Methods. 15:191-200; 2009.

55.	Moran, E. C.; Baptista P. M.; Evans, D. W.; Soker, S.; Sparks, J. L. Evaluation of parenchymal fluid pressure in native and decellularized liver tissue. Biomed. Sci. Instrum. 48:303-309; 2012.

56.	Murry, C. E.; Pu W. T. Reprogramming fibroblasts into cardiomyocytes N. Engl. J. Med. 364:177-178; 2011.

57.	Nagata, H.; Nishitai, R., Shirota, C.; Zhang, J. L.; Koch, C. A.; Cai, J.; Awwad, M.; Schuurman, H. J.; Christians, U.; Abe, M.; Baranowska-Kortylewicz. J.; Platt, J. L.; Fox, I. J. Prolonged survival of porcine hepatocytes in cynomolgus monkeys. . Gastroenterology 132:321-329; 2007.

58.	Nahmias, Y.; Berthiaume, F.; Yarmush, M. L. Integration of technologies for hepatic tissue engineering. Adv. Biochem. Eng. Biotechnol. 103:309-329; 2007.

59.	Nakamura, T.; Ohmori, K.; Kanemaru, S. Tissue-engineered airway and ‘in situ tissue engineering’. Gen. Thorac. Cardiovasc. Surg. 59:91-97; 2011.

60.	Nakayama, K. H.; Batchelder C. A.; Lee, C. I.; Tarantal, A. F. Decellularized rhesus monkey kidney as a three-dimensional scaffold for renal tissue engineering. Tissue Eng. Part A 16:2207- 2216; 2010.

61.	Ohashi, K.; Yokoyama, T.; Yamato, M.; Kuge, H.; Kanehiro, H.; Tsutsumi, M.; Amanuma, T.; Iwata, H.; Yang, J.; Okano, T.; Nakajima, Y. Engineering functional two- and three-dimensional liver systems in vivo using hepatic tissue sheets. Nat. Med. 13:880-885; 2007.

62.	Oliveira, A. C.; GarzÓn, I.; Ionescu, A. M.; Carriel, V.; Cardona, J. de L.; González-Andrades, M.; Pérez Mdel, M.; Alaminos, M., Campos, A. Evaluation of small intestine grafts decellularization methods for corneal tissue engineering. . PLoS One 8:e66538; 2013.

63.	Ott, H. C.; Clippinger, B.; Conrad, C.; Schuetz, C.; Pomerantseva, I.; Ikonomou, L.; Kotton, D.; Vacanti, J. P. Regeneration and orthotopic transplantation of a bioartificial lung. Nat. Med. 16:927-933; 2010.

64.	Ott, H. C.; Matthiesen T. S.; Goh, S. K.; Black, L. D.; Kren, S. M.; Netoff, T. I.; Taylor, D. A. Perfusion-decellularized matrix: using nature’s platform to engineer a bioartificial heart. Nat. Med. 14:213-221; 2008.

65.	Patel, N.; S. E., Picciani, R.; Cavett, V.; Caldwell-Busby, J. A.; Bhattacharya, S. K. Strategies to recover proteins from ocular tissues for proteomics. Proteomics 8:1055-1070; 2008.

66.	Petersen, T. H.; Calle, E. A.; Zhao, L.; Lee, E. J.; Gui, L.; Raredon, M. B.; Gavrilov, K.; Yi, T.; Zhuang, Z.W.; Breuer, C.; Herzog, E.; Niklason, L. E. Tissue-engineered lungs for in vivo implantation. Science 329:538-541; 2010.

67.	Prasertsung, I.; Kanokpanont, S.; Bunaprasert, T.; Thanakit, V.; Damrongsakkul, S. Development of acellular dermis from porcine skin using periodic pressurized technique. J. Biomed. Mater. Res. B Appl. Biomater. 85:210-219; 2008.

68.	Price, A. P.; England, K. A.; Matson, A. M.; Blazar, B. R.; Panoskaltsis- Mortari, A. Development of a decellularized lung bioreactor system for bioengineering the lung: the matrix reloaded. Tissue Eng. Part A 16:2581-2591; 2010.

69.	Reing, J. E.; Brown, B. N.; Daly, K. A.; Freund, J. M.; Gilbert, T. W.; Hsiong, S. X.; Huber, A.; Kullas, K.E.; Tottey, S.; Wolf, M. T.; Badylak, S. F. The effects of processing methods upon mechanical and biologic properties of porcine dermal extracellular matrix scaffolds. Biomaterials 31:8626-8633; 2010.

70.	Rieder, E.; Kasimir, M. T.; Silberhumer, G.; Seebacher, G.; Wolner, E.; Simon, P.; Weigel, G. Decellularization protocols of porcine heart valves differ importantly in efficiency of cell removal and susceptibility of the matrix to recellularization with human vascular cells. J. Thorac. Cardiovasc. Surg. 127:399-405; 2004.

71.	Roh, J. D.; Nelson, G.N.; Udelsman, B.V.; Brennan, M. P.; Lockhart, B.; Fong, P.M.; Lopez-Soler, R.I.; Saltzman, W. M.; Breuer, C.K. Centrifugal seeding increases seeding efficiency and cellular distribution of bone marrow stromal cells in porous biodegradable scaffolds. Tissue Eng. 13:2743-2749; 2007.

72.	Rosario, D. J.; Reilly G. C.; Ali Salah, E.; Glover, M.; Bullock, A. J.; Macneil, S. Decellularization and sterilization of porcine urinary bladder matrix for tissue engineering in the lower urinary tract. Regen. Med. 3:145-156; 2008.

73.	Sadr, N.; Pippenger, B. E.; Scherberich, A.; Wendt, D.; Mantero, S.; Martin, I. Papadimitropoulos A. Enhancing the biological performance of synthetic polymeric materials by decoration with engineered, decellularized extracellular matrix. Biomaterials 33:5085-5093; 2012.

74.	Sano, M. B.; Neal, R. E. 2nd; Garcia, P. A.; Gerber, D.; Robertson, J.; Davalos, R. V. Towards the creation of decellularized organ constructs using irreversible electroporation and active mechanical perfusion. Biomed. Eng. Online 9:83-99; 2010.

75.	Schechner, J. S.; Crane S. K.; Wang, F.; Szeglin, A. M.; Tellides, G.; Lorber, M. I.; Bothwell, A. L.; Pober, J. S. Engraftment of a vascularized human skin equivalent. FASEB J. 17:2250-2256; 2003.

76.	Schenke-Layland, K.; Vasilevski, O.; Opitz, F.; König, K.; Riemann, I.; Halbhuber, K. J.; Wahlers, T.; Stock, U. A. Impact of decellularization of xenogeneic tissue on extracellular matrix integrity for tissue engineering of heart valves. J. Struct. Biol. 143:201-208; 2003.

77.	Seddon, A. M.; Curnow, P.; Booth, P. J. Membrane proteins, lipids and detergents: not just a soap opera. Biochim. Biophys. Acta 1666:105-117; 2004.

78.	Shirakigawa, N.; Ijima, H.; Takei, T. Decellularized liver as a practical scaffold with a vascular network template for liver tissue engineering. J. Biosci. Bioeng. 114:546-551; 2012.

79.	Shupe, T.; Williams, M.; Brown, A.; Willenberg, B.; Petersen, B. E. Method for the decellularization of intact rat liver. Organogenesis 6:134-136; 2010.

80.	Simionescu, D. T.; Lovekamp, J. J.; Vyavahare, N. R. Degeneration of bioprosthetic heart valve cusp and wall tissues is initiated during tissue preparation: an ultrastructural study. J. Heart Valve Dis. 12:226-234; 2003.

81.	Song, J. J.; Kim, S.; Liu, Z.; Madsen, J. C.; Mathisen, D. J.; Vacanti, J. P.; Ott, H. C. Enhanced in vivo function of bioartificial lungs in rats. Ann. Thorac. Surg. 92:998-1005; 2011.

82.	Song, J. J.; Ott, H. Bioartificial lung engineering. Am. J. Transplant. 12:283-288; 2012.

83.	Song, J. J.; Ott, H. Organ engineering based on decellularized matrix scaffolds. . Trends Mol. Med. 17:424-432; 2011.

84.	Soto-Gutierrez, A.; Yagi, H.; Uygun, B.E.; Navarro-Alvarez, N.; Uygun, K.; Kobayashi, N.; Yang, Y. G.; Yarmush, M. L. Cell delivery: from cell transplantation to organ engineering. Cell Transplant. 19:655-665; 2010.

85.	Soto-Gutierrez, A.; Zhang, L.; Medberry, C.; Fukumitsu, K.; Faulk, D.; Jiang, H.; Reing, J.; Gramignoli, R.; Komori, J.; Ross, M.; Nagaya, M.; Lagasse, E.; Stolz, D.; Strom, S. C.; Fox, I. J.; Badylak, S. F. A wholeorgan regenerative medicine approach for liver replacement. Tissue Eng. Part C Methods 17:677-689; 2011.

86.	Stapleton, T. W.; Ingram, J.; Katta, J.; Knight, R.; Korossis, S.; Fisher, J.; Ingham, E. Development and characterization of an acellular porcine medial meniscus for use in tissue engineering. Tissue Eng. Part A 14:505-518; 2008.

87.	Takahashi, K.; Yamanaka, S. Induction of pluripotent stem cells from mouse embryonic and adult ﬁbroblast cultures by deﬁned factors. Cell 126:663-676; 2006.

88.	Tandon, N.; Marsano, A.; Cannizzaro, C.; Voldman, J.; Vunjak-Novakovic, G. Design of electrical stimulation bioreactors for cardiac tissue engineering. In Conference Proceedings: Annual International Conference of the IEEE Engineering in Medicine and Biology Society 2008:3594-3597; 2008.

89.	Toni, R.; Tampieri, A.; Zini, N.; Strusi, V.; Sandri, M.; Dallatana, D.; Spaletta, G.; Bassoli, E.; Gatto, A.; Ferrari, A.; Martin, I. Ex situ bioengineering of bioartificial endocrine glands: a new frontier in regenerative medicine of soft tissue organs. Ann. Anat. 193:381-394; 2011.

90.	Traverse, J. H.; Henry, T.; Ellis, S. G.; Pepine, C.J.; Willerson, J. T.; Zhao, D. X.; Forder, J. R.; Byrne, B. J.; Hatzopoulos, A. K.; Penn, M. S.; Perin, E. C.; Baran, K. W.; Chambers, J.; Lambert, C.; Raveendran, G.; Simon, D. I,; Vaughan, D. E.; Simpson, L. M.; Gee, A. P.; Taylor, D. A.; Cogle, C. R.; Thomas, J. D.; Silva, G. V,; Jorgenson, B. C.; Olson, R. E.; Bowman, S.; Francescon, J.; Geither, C.; Handberg, E.; Smith, D. X.; Baraniuk, S.; Piller, L. B.; Loghin, C.; Aguilar, D.; Richman, S.; Zierold, C.; Bettencourt, J.; Sayre, S. L.; Vojvodic, R. W.; Skarlatos, S. I.; Gordon, D. J.; Ebert, R. F.; Kwak, M.; Moyé, L. A.; Simari,  R. D. Cardiovascular Cell Therapy ResearchNetwork. Effect of intracoronary delivery of autologous bone marrow mononuclear cells 2 to 3 weeks following acute myocardial infarction on left ventricular function: the LateTIME randomized trial. JAMA 306:2110-2119; 2011.

91.	Uygun, B. E.; Sotto-Gutierrez, A.; Yagi, H.; Izamis, M. L.; Guzzardi, M. A.; Shulman, C.; Milwid, J.; Kobayashi, N.; Tilles, A.; Berthiaume, F.; Hertl, M.; Nahmias, Y.; Yarmush, M. L.; Uygun, K. Organ reengineering through development of a transplantable recellularized liver graft using decellularized liver matrix. Nat. Med. 16:814-820; 2010.

92.	Villalona, G. A.; Udelsman, B.; Duncan, D. R.; McGillicuddy, E.; Sawh- Martinez, R. F.; Hibino, N.; Painter, C.; Mirensky, T.; Erickson, B.; Shinoka, T.; Breuer, C. K. Cell-seeding techniques in vascular tissue engineering. Tissue Eng. Part B Rev. 16:341-350; 2010.

93.	Volkmer, E.; Drosse, I.; Otto, S.; Stangelmayer, A.; Stengele, M.; Kallukalam, B. C.; Mutschler, W.; Schieker, M. Hypoxia in static and dynamic 3D culture systems for tissue engineering of bone. Tissue Eng. Part A 14:1331-1340; 2008.

94.	Voytik-Harbin, S. L.; Brightman, A. O.; Kraine, M. R.; Waisner, B.; Badylak, S. F. Identification of extractable growth factors from small intestinal submucosa. J. Cell. Biochem. 67:478-491; 1997.

95.	Wang, S.; Nagrath, D.; Chen, P. C.; Berthiaume, F.; Yarmush, M. L. Three-dimensional primary hepatocyte culture in synthetic self-assembling peptide hydrogel. Tissue Eng. Part A 14:227-236; 2008.

96.	Weinand, C.; Xu J.; Peretti, G. M.; Bonassar, L. J.; Gill, T. J. Conditions affecting cell seeding onto three-dimensional scaffolds for cellular-based biodegradable implants. J. Biomed. Mater. Res. B Appl. Biomater. 91:80-87; 2009.

97.	Woods, T.; Gratzer, P. Effectiveness of three extraction techniques in the development of a decellularized bone-anterior cruciate ligament- bone graft. Biomaterials 26:7339-7349; 2005.

98.	Xia, Y.; Prawirasatya, M.; Heng, B. C.; Boey, F.; Venkatraman, S. S. Seeding density matters: extensive intercellular contact masks the surface dependence of endothelial cell-biomaterial interactions. J. Mater. Sci. Mater. Med. 22:389-396; 2011.

99.	Yang B,; Zhang, Y.; Zhou, L.; Sun, Z.; Zheng, J.; Chen, Y.; Dai, Y. Development of a porcine bladder acellular matrix with well-preserved extracellular bioactive factors for tissue engineering. Tissue Eng. Part C Methods 16:1201-1211; 2010.

100.	Yang, Y. G.; Sykes, M. Xenotransplantation: current status and a perspective on the future. Nat. Rev. Immunol. 7:519-531; 2007.

Figure legend

Figure 1. Rationale of tissue decellularization. The cell-free scaffold can originate from the decellularization of native material or from synthesized material. The resulting scaffold can be directly transplanted into a patient (1), relying on its capacity to stimulate cells towards endogenous tissue repair (2). (3) In addition, prior to implantation, the ECM can be seeded with cells that guide the material (to enhance remodeling or vascularization) or have a specific function (proliferation or differentiation).